## Slide 1: Optical and X-Ray Charactorization of Ge1-ySny alloy on GaAs
Haley Woolf,1 Matt Kim,2 Carola Emminger,1 Carlos Armenta,1 Stefan Zollner1
Department of Physics, NMSU, Las Cruces, NM
QuantTera, Scottsdale, AZ
College of Arts and Science
Department of Physics
FA9550-20-1-0135
This work was supported by Air Force Office of Scientific Research under award number FA9550-20-1-0135.

## Slide 2: Outline
Background:
  UV ellipsometry and x-ray diffraction
Abstract
X-ray diffraction data:
  Omega rocking curves, and reciprocal pace maps on (004), (224), &
Lattice constants
Optical data:
  Pseudodielectric function, optical constants, & 2nd der. of dielectric function
Theoretical E1 & E1+Δ1 with tin content
Conclusion
1

## Slide 3: Background
X-ray diffraction uses Bragg’s Law to determine the characteristics of different materials. Omega Rocking curves were used to determine the lattice constants and reciprocal space maps were used to determine the strain and relaxation.
Bragg’s Law:
Distance between layers of atoms
Angle between incident beam and the surface of the crystal
Wavelength of the rays
2

## Slide 4: Background
In UV ellipsometry, light is reflected/transmitted from a material causing the polarization to change. ψ is the amplitude ratio and Δ is the phase difference of the light. ψ and Δ depend on the material’s optical properties and thicknesses.
3

## Slide 5: Introduction
Ge1-ySny layer is 1600 nm thick and was grown on GaAs by chemical vapor epitaxy. The tin content can be found with (004) reciprocal space map and omega rocking curves.
and reciprocal space maps will determine the strain and relaxation of the epitaxial layer
UV ellipsometry can determine the sample’s optical properties, including the dielectric function and the optical constants.
GeSn is often used in lasers and inferred detectors.
GaAs
Ge1-ySny
Oxide
Pseudomorphic/strained epitaxial layer
Relaxed epitaxial layer
4

## Slide 6: (004) Rocking Curves (Open Detector)
FWHM
Bulk Ge 0.0074°
GaAs 0.0098°
GeSn 0.0155°
Bulk GaAs 0.0076°
Braggs’s Law:
Lattice Constant:
GeSn= 5.679 Å
GaAs = 5.653 Å
Ge = 5.658 Å
Sn = 6.489 Å
5

## Slide 7: (004) Reciprocal Space Maps
Dashed line drawn through substrate peak
M-Mosaic Spread (Relaxation Line)
Bulk GaAs
Bulk Ge
GeSn on GaAs
6

## Slide 8: & Rocking Curve (Open Detector):
FWHM
Bulk Ge: 0.0109°
GaAs: 0.0117°
GeSn: 0.0225°
Bulk GaAs: 0.0114°
FWHM
Bulk Ge: 0.0149°
GaAs: 0.0221°
GeSn: 0.0281°
Bulk GaAs: 0.0125°
Grazing Exit:
Grazing Incidence:
7
X-ray tube
Detector
X-ray tube
Detector

## Slide 9: (224) Grazing Incidence Reciprocal Space Map
W-Wavelength Streak
M-Mosaic Spread (Relaxation Line)
Black line drawn from origin (Relaxed)
Dashed line drawn through substrate peak (Pseudomorphic)
Bulk GaAs
Bulk Ge
GeSn on GaAs
8

## Slide 10: Grazing Exit Reciprocal Space Map
W-Wavelength Streak
M-Mosaic Spread (Relaxation Line)
Black line drawn from origin (Relaxed)
Dashed line drawn through substrate peak (Pseudomorphic)
Bulk GaAs
Bulk Ge
GeSn on GaAs
9

## Slide 11: Lattice Constants
With Vegard’s law and continuum elasticity theory, the tin content of the Ge1-ySny layer can be found with the measured and known lattice constants of GaAs, Ge, and Sn.
|| substrate= 5.653 Å
Poisson Ratio:
GeSn= 5.679 Å
GaAs = 5.653 Å
Ge = 5.658 Å
Sn = 6.489 Å
Vegard’s Law:
If layer is fully relaxed, the % Sn is 2.6%
If layer is fully strained, the % Sn is 1.2%
Bragg’s Law:
Pseudomorphic
Condition
GeSn= 5.679 Å
||
10
Notes: With Vegard’s law and continuum elasticity theory, the tin content of the Ge1-ySny layer can be found with the measured and known lattice constants of GaAs, Ge, and Sn.

## Slide 12: Pseudodielectric Function Before/After Cleaning
The Ge1-ySny on GaAs sample was cleaned ultrasonically with water and then isopropanol to remove organic layers and most of the native oxide.
 | Oxide Thickness
As Received (May 20th): | 43.66 Å
Before Cleaning (June 14th): | 72.07 Å
After Cleaning (June 14th): | 26.50 Å
After 2nd Cleaning (June 15th): | 25.90 Å
11

## Slide 13: Pseudodielectric Function and Optical Constants
GaAs
Ge1-ySny
Oxide
MODEL
Air
12

## Slide 14: 2nd Derivative of the Dielectric Function
By fitting the 2nd derivative of the dielectric function, the critical point parameters were found. This includes energy, amplitude, phase angle, broadening, and the line shape. The phase angle for E1 and E1+Δ1 were fixed to be the same.
Critical Points of Ge (Orange)
CP | E (eV) | A | Φ (deg) | Γ (meV) | n
E1 | 2.118 | 5.73 | 248 | 0.048 | 0
E1+Δ1 | 2.269 | 5.43 | 248 | 0.088 | 0
E’0 | 3.155 | 1.32 | 224 | 0.115 | 0
E’0+Δ’0 | 3.324 | 0.873 | 235 | 0.103 | 0
E2 | 4.329 | 13.1 | 310 | 0.121 | 0
Critical Points of GeSn (Blue)
CP | E (eV) | A | Φ (deg) | Γ (meV) | n
E1 | 2.113 | 5.32 | 246 | 0.050 | 0
E1+Δ1 | 2.314 | 3.53 | 246 | 0.066 | 0
E’0 | 3.099 | 1.33 | 175 | 0.102 | 0
E’0+Δ’0 | 3.344 | 0.486 | 266 | 0.139 | 0
E2 | 4.354 | 11.2 | 318 | 0.097 | 0
13
Notes: By fitting the 2nd derivative of the dielectric function, the critical point parameters were found. This includes energy, amplitude, phase angle, broadening, and the line shape. The phase angle for E1 and E1+Δ1 were fixed to be the same.

## Slide 15: Theoretical E1 & E1+Δ1 with Tin Content
The marked squares are the measured energies of bulk Ge and the Ge1-ySny epitaxial layer. The Ge1-ySny energy for the E1 is slightly higher.
Relaxed:
Strained:
eV,
eV,
eV,
eV,
small shear approximation
14

## Slide 16: Conclusion
The (224) reciprocal space maps showed that the GeSn epitaxial layer was grown pseudomorphically (fully strained).
Using Vegard’s Law, continuum elasticity theory, and the (004) reciprocal space map, the tin content is found to be y=0.012.
After cleaning the sample, the thickness of the oxide was reduced to 26 Å
Using the ellipsometry data, the fitted GeSn dielectric function was similar to bulk Ge most likely because of the low tin content.
The fit second derivative of the dielectric function helped find the critical point parameters and compared to bulk Ge
The energy for the E1 is slightly higher in the GeSn layer despite theory.
Ge1-ySny
15

## Slide 17: Questions?

## Slide 18: References
[1] P. F. Fewster, X-ray scattering from semiconductors. London: World Scientific (2016)
[2] N.S. Fernando, R.A. Carrasco, R. Hickey, J. Hart, R. Hazbun, S. Schoeche, J.N. Hilfiker, J. Kolodzey, and S. Zollner, Band gap and strain engineering of pseudomorphic Ge1-x-ySixSnyalloys on Ge and GaAs for photonic applications, J. Vac. Sci. Technol. B 36, Mar/Apr (2018).
[3] N.S. Fernando, T.N. Nunley, A. R. Ghosh, C.M. Nelson, J.A. Cooke, A.A. Medina, S. Zollner, C. Xu, J. Menendez, and J. Kouvetakis, Temperature dependence of the interband critical points of bulk Ge and strained Ge on Si, Applied Surface Science 421, 905-912 (2017).
[4] T.N. Nunley, N.S. Fernando, N. Samarasingha, J.M. Moya, C.M. Nelson, A.A. Medina, and S. Zollner, Optical constants of germanium and thermally grown germanium dioxide from 0.5 to 6.6 eV via a multi-sample ellipsometry investigation, J. Vac. Sci. Technol. B 34, 061205 (2016).
[5] H.G. Tompkins, and J.N. Hilfiker. Spectroscopic Ellipsometry: Practical Application to Thin Film Characterization, Momentum Press (2016).