## Slide 1: Temperature Dependence of the Direct Bandgap of InSb
Melissa Rivero Arias, Carola Emminger, Cesy M. Zamarripa,
Jaden R. Love, and Stefan Zollner
College of Arts and Sciences, Department of Physics
URCAS, April 2022
FA9550-20-1-0135

## Slide 2: Outline
Scientific language
What is InSb?
Electromagnetic spectrum and band gap
Expectations
Experiment, equipment and sample preparation
Data and corrections
Analysis
Conclusions and future work

## Slide 3: Temperature Dependence of the Direct Bandgap of InSb
Undergraduate, Department of Physics
Experiments that go to low and/or high temperatures
Minimum amount of energy required for an electron to break free of its ground state
Indium Antimonide: narrow-gap semiconductor material from the III-V group
3
Melissa Rivero
In collaboration with: Dr. Stefan Zollner, Carola Emminger, Cesy Zamarripa and Jaden R. Love
College of Arts and Sciences, Department of Physics
URCAS, April 2022
3

## Slide 4: What is InSb?
Indium Antimonide: narrow-gap semiconductor material from the III-V group.
Examples (III-V):
GaSb (gallium antimonide)
InAs (indium arsenide)
GaP (gallium phosphide)

## Slide 5: What is InSb?
Used in infrared detectors, including thermal imaging cameras, FLIR systems, infrared homing missile guidance systems, and in infrared astronomy.

## Slide 6: Electromagnetic Spectrum
Range of frequencies of electromagnetic radiation and their respective wavelengths and photon energies.
J.A. Woollam IR-VASE
J.A. Woollam V-VASE

## Slide 7: Band Gap
The band gap is the minimum amount of energy required for an electron to break free of its bound state. When the band gap energy is met, the electron is excited into a free state, and can therefore participate in conduction.
InSb

## Slide 8: Expectations (1/3)
Measurement of the dielectric function of bulk InSb from 80 to 700 K near the direct band gap (E0)
80 to 700 Kelvin
-193.5 to 426.85 Celsius
-315.67 to 800.33 Fahrenheit
Bulk InSb
Comparison
Direct Bandgap at 300 K (room temperature): ~0.17 eV

## Slide 9: Expectations (2/3)
Using FTIR spectroscopic ellipsometry in an ultra-high vacuum (UHV) cryostat with diamond windows.
Cryostat with diamond windows
J.A. Woollam IR-VASE
Energies: 1.24 meV to 1.7 eV
VIS-UV and FTIR spectra (dielectric functions) After oxide correction

## Slide 10: Expectations (3/3)
Calculations indicate that InSb should undergo a topological phase transition from semiconductor to semi-metal (and topological insulator) at 600 K (negative band gap).
Negative Bandgap (at high temps)

## Slide 11: Experiment and Equipment
Cryostat with diamond windows
J.A. Woollam IR-VASE
J.A. Woollam V-VASE
Oxide and organic layers
InSb
Spectroscopic Ellipsometry
Non-destructive, noncontact, and non-invasive optical technique based on the change in the polarization state of light as it is reflected obliquely from a thin film sample.
Uses a model-based approach to determine thin film, interface, and surface roughness thicknesses, as well as optical properties.
Notes: Rotating compensator ellipsometer

## Slide 12: Sample preparation
InSb cleaning process (on a Branson Ultrasonic Cleaner):
Indium antimonide sample was cleaned using water and isopropanol on the ultrasonic cleaner for 15 minutes on each to remove organic layers before the temperature dependent ellipsometry measurements.
 | Oxide Thickness (Å)
Before Clean | 28.2
After Clean | 22.5

## Slide 13: Data and Corrections
= Bandgap
Pseudo Dielectric Functions (“raw” data)

## Slide 14
Oxide Correction

## Slide 15
Dielectric Functions

## Slide 16
Pseudo Dielectric Functions (“raw” data)
+
Oxide Correction
=
Dielectric Functions

## Slide 17: Analysis
How did the bandgap change through temperatures?
Tauc Plot:
Parametric-Semiconductor Model:
*Computed manually*
*Based on computer model*
Need linear region, not possible

## Slide 18: Direct Bandgap vs. Temperature
Bose-Einstein Model
Band gap
Broadening
]

## Slide 19: Conclusions
Dielectric function of InSb was measured from 80 to 700K with an oxide correction of 25 +/- 5 Å
Band gap is difficult to determine:
1. Parametric semiconductor model shows great results
Band gap shrinks with increasing temperature:
1. Follows Bose-Einstein relationship up to 300 K, stays constant up to 550 K and increases with temperature.
2. Thermal excitation of electron hole pairs.
First measurements of InSb band gap above 300 K
InSb would behave as a topological insulator above melting point. Not possible.
Burstein-Moss shift
Notes: Birstein-Moss shift

## Slide 20: Direct Bandgap vs. Temperature
Experimental data
Expected behavior

## Slide 21: Sad ending
Unfortunately, the InSb sample melted at 750 K, but melting point is 800 K…
Before
After
Future work:
Repeat experiment at high temperatures below 750 K

## Slide 22: Thank you! Questions?

## Slide 23: References
[1] C. L. Littler and D. G. Seiler, Appl. Phys. Lett. 46, 986 (1985).
[2] S. T. Schaefer, S. Gao, P. T. Webster, R. R. Kosireddy, and S. R. Johnson, J. Appl. Phys. 127, 165705 (2020).
[3] http://www.ioffe.ru/SVA/NSM/Semicond/InSb/bandstr.html
[4] S. Zollner, S. Gopalan, and M. Cardona, Solid State Commun., 77, 485 (1991).

## Slide 24
https://www.pveducation.org/pvcdrom/pn-junctions/band-gap
http://www.ioffe.ru/SVA/NSM/Semicond/InSb/bandstr.html
https://www.horiba.com/ind/scientific/technologies/spectroscopic-ellipsometry/spectroscopic-ellipsometry/
http://solidstate.mines.edu/videonotes/VN_9_3.pdf
https://en.wikipedia.org/wiki/Infrared
https://energyeducation.ca/encyclopedia/Band_gap