## Slide 1: Intravalence Band Transitions in Gapless Topological Insulators
Stefan Zollner
Head, Department of Physics
New Mexico State University Las Cruces, NM, USA
Supported by AFOSR SFFP and FA9550-20-1-0135.
FA9550-20-1-0135
FA9550-20-F-0005
Email: zollner@nmsu.edu. WWW: http://femto.nmsu.edu.
12 two-hour lectures on YouTube.

## Slide 2
Biography
Regensburg/Stuttgart
Germany
NMSU
Las Cruces, NM
Since 2010
Motorola (Mesa, Tempe)
Arizona, 1997-2005
Motorola, Freescale
Texas, 2005-2007
Freescale, IBM
New York, 91-92; 07-10
92-97

## Slide 3: Where is Las Cruces, NM ???
White Sands NP
Stefan Zollner, 2023

## Slide 4: New Mexico State University, Las Cruces
Stefan Zollner, 2023
Land grant institution, Carnegie R2 Comprehensive: Arts and Sciences, Education, Business, Agriculture
Ph.D. programs in sciences, engineering, agriculture; Ag extension
14,000 students (11,500 UG, 2,500 GR), 1000 faculty
Minority-serving, Hispanic-serving (60% Hispanic/NA, 26% White)
Small-town setting
Military-friendly institution (Army and Air Force ROTC programs)
Community engagement classification (first-generation students, Pell grant recipients)
Physics: BS/BA, MS, PhD degrees. 71 UG and 37 GR students.
12 faculty (HE Nuclear and Materials Physics), 1.7 M$ expenditures. ABET-accredited BS in Physics and BS in Engineering Physics

## Slide 5: Announcement: Special Issue on SiGeSn Alloys
Stefan Zollner, 2023
There will be a special issue on Silicon-Germanium-Tin Alloys in
The Journal of Vacuum Science and Technology B.
Watch for the announcement.
Manuscripts will be due in late fall or early spring.
Guest Editors: Gernot Pomrenke (AFOSR), Tania Paskova (ARO), Chip Claflin (AFRL), etc.

## Slide 6: What is a Topological Insulator?
Nature web site: “Topological insulators are materials that are insulating in their interior but can support the flow of electrons on their surface. The underlying cause is time-reversal symmetry: their physics is independent of whether time is flowing backward or forward.”
Parity reversal of bands (p-s-p) is a key ingredient of topological insulators.
A topological space X is a set of points with a family (called topology) of subsets (called open sets) with the following properties:
The empty set and X itself are open.
Any arbitrary (finite or infinite) union of open sets is open.
The intersection of any finite open sets is open.
The complement of an open set is called closed.
Wikipedia: “The most general type of a mathematical space that allows for the definition of limits, continuity, and connectedness.”
Stefan Zollner, 2023
p

## Slide 7: Intravalence Band Transitions in Gapless Semiconductors
Bonds and Bands
Band Structure of Silicon, Germanium, and a-Tin
Why is a-Tin a Topological Insulator?
Intravalence Band Absorption in Ge and AlSb
Intravalence Band Absorption in a-Tin
Dependence on Temperature, Substrate, and Doping with Ge
Summary
Stefan Zollner, 2023
Woollam FTIR-VASE;
cryostat with CVD diamond windows
10-800 K

## Slide 8: Bohr Model for the Hydrogen Atom
Stefan Zollner, 2023
Quantum Numbers:
n 1,2,3,…
l 0,…,n-1
m -l,…,l
s +/- 1/2
Relativistic corrections:
s electrons (l=0) close to the core (Darwin shift)
J=L+S total angular momentum
Spin-orbit coupling L·S
L=1, S=1/2 J=1/2 or 3/2
E(n)=-R/n2
R=13.6 eV
Notes: Birstein-Moss shift

## Slide 9: Bonding and Anti-Bonding Orbitals
s: Y=y1+y2
s*: Y=y1-y2
px, py, pz
p*
p
C electronic configuration: 1s2 2s2 2p2
L shell forms sp3 hybrid: 1s2 2s1 2p3
Valence Band
Conduction Band
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 10: Bonds and Bands
10
Fox, Chapter 3
Works well for Ge, GaAs, etc.
Add kinetic energy
Stefan Zollner, 2023

## Slide 11: Periodic Table of the Elements
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 12: A simple band structure for Germanium
p
s
s*
p*
VB
filled
CB
empty
EF
Add spin-orbit coupling: J=L+S
Add kinetic energy
s
s*
j=1/2
j=3/2
j=1/2
j=3/2
D0
D0’
Ge electronic configuration: … 4s2 4p2
N shell forms sp3 hybrid: … 4s1 4p3
K=mv2/2=p2/2m
=2k2/2m
m: effective mass
CB (empty)
e
so
D0
hh
lh
4s VB
E
Momentum k
EF
E0 band gap
filled
filled
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 13: Band structure of Germanium
p
s
s*
p*
filled
empty
EF
Add spin-orbit coupling: J=L+S
Add FCC symmetry
s
s*
j=1/2
j=3/2
j=1/2
j=3/2
D0
D0’
Ge electronic configuration: … 4s2 4p2
N shell forms sp3 hybrid: … 4s1 4p3
E
Momentum k
filled
FCC Brillouin zone
Band structure
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 14: Examples of Band Structures: Si and Ge
Stefan Zollner, 2023, AFRL Lectures Series 3
Total Energy: E=K+V, K=p2/2m. p=0 corresponds to G-point in BZ.
Four valence electrons per atom: 3s2, 3p2 (8 e- per primitive cell)
Symmetry labels are representations from the point group.
(111)
(100)
(110)
s
p
p
p*
VB
gap
s*
s
p*
CB
s*
Darwin shift

## Slide 15: Dirac Points in Silicon and Germanium
Need “extra representations” for Ge because of strong spin effects.
15
Yu and Cardona, Fundamentals of Semiconductors (Springer, 2010)
Stefan Zollner, 2023

## Slide 16: Topological Differences Between Ge and GaAs
Stefan Zollner, 2023
Ge
GaAs
Bands cross: different symmetries.
Dirac point: Linear dependence on k
Inversion symmetry leads to crossing.
Bands repel: same symmetry.
Anti-crossing due to interactions.
No degeneracy at the X-point.

## Slide 17: Atomic Radius
Atomic radius decreases to the right, increases downward.
Relativistic effects increase downward.
Ge and Sn have d-electrons, C and Si do not.
IV
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 18: Relativistic Effects: Darwin Shift: C, Si, Ge, Sn
The s* band moves down, as the elements get heavier.
In a-tin, the s* band moves into the p-band manifold, between the j=1/2 and j=3/2 states.
This makes a-tin an (inverted) gapless semiconductor.
j=1/2
j=3/2
p
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 19: Band Inversion: Topological Insulators
Stefan Zollner, 2023, AFRL Lectures Series 1
Germanium
p
s*
a-tin
p
p
p*
s*
j=1/2
j=3/2
Band gap must be zero.
Symmetry inversion in VB.
Linear crossing
(Dirac point)
Inversion Symmetry
Gapless Semiconductor

## Slide 20: Optical Interband Transitions in a-Tin
Stefan Zollner, 2023
R.A. Carrasco, APL 113, 232104 (2018).
L-electron
light “hole”
heavy hole
DEGL»0
“electron”
split-off hole
Spectroscopic Ellipsometry
Dielectric Function

## Slide 21: Topological Features of a-Tin under Strain
Stefan Zollner, 2023
R.A. Carrasco, APL 113, 232104 (2018).
Topological phase transition from Dirac-semimetal to topological insulator as a function of strain.
Strain can be tuned by growing on substrates with different lattice constants (InSb, CdTe, CdZnTe) or by doping with Ge.
335 RSM
004
compressive
tensile
Dirac point
Indirect
gap
Direct gap
400 cm-1
Warping
unstrained

## Slide 22: Interband Transitions in Ge
Stefan Zollner, 2023, AFRL Lectures Series 3
Optical (reduced) mass m
Watch the signs for inverted semiconductors.
Fox, Chapter 3
3
Optical mass follows from crystal momentum conservation.

## Slide 23: Fermi’s Golden Rule: Tauc Plot
Stefan Zollner, 2023
Use k·p matrix element P: EP=2P2/m0
23
Direct band gap absorption
The Tauc plot is wishful thinking.
No linear region:
1/E2 denominator
Broadening
Excitons
Nonparabolicity
Melissa Rivero Arias
Do not recommend the Tauc plot to find band gaps (no obvious linear region).
Notes: Birstein-Moss shift

## Slide 24: Bohr model for free excitons
Electron and hole form a bound state with binding energy.
RH=13.6 eV Rydberg energy.
QM mechanical treatment easy.
Reduced electron/hole mass (optical mass)
Static screening with static dielectric constant er.
Exciton radius: aH=0.53 Å
Excitons stable if EX>>kT ????
Exciton momentum is zero.
Exciton enhancement important even if EX<<kT.
Stefan Zollner, 2023

## Slide 25: Sommerfeld enhancement
Stefan Zollner, 2023
Excitonic Rydberg energy
Discrete states
Discrete absorption
Continuum absorption
R. J. Elliott, Phys. Rev. 108, 1384 (1957)
Yu & Cardona
Use Bohr wave functions to calculate e2.
Toyozawa discusses broadening.

## Slide 26: Ge: Elliott-Tanguy Exciton Absorption
Stefan Zollner, 2023, AFRL Lectures Series 3
Direct band gap absorption
Excitonic binding energy: R=RH×mh/es2
´
bound excitons
exciton continuum enhancement
Tanguy’s contributions:
Add Lorentzian broadening
Kramers-Kronig transform to get the real part.
R. J. Elliott, Phys. Rev. 108, 1384 (1957).
Christian Tanguy, Phys. Rev. Lett. 75, 4090 (1995) + (E)
Notes: Birstein-Moss shift

## Slide 27: Calculation of Absorption Spectrum from k.p Theory
Can we calculate the absorption spectrum?
Yes, we can for Ge in the low carrier density limit.
It does not work (yet) for other III/V compounds.
Carola Emminger et al., JAP 131, 165701 (2022).
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 28: Elliott-Tanguy Theory Applied to Ge
ε1
ε2
Fixed parameters:
  Electron and hole masses (temperature dependent)
  Excitonic binding energy R
  Amplitude A (derived from matrix element P)
Adjustable parameters:
  Broadening Γ: 2.3 meV
  Band gap E0
  Linear background A1 and B1 (contribution from E1 to real part of e)
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Quantitative agreement
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 29: Elliott-Tanguy Theory Applied to Ge
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
??? at high T.
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
Stefan Zollner, 2023
Notes: Birstein-Moss shift

## Slide 30: Interband Transitions
Stefan Zollner, 2023, AFRL Lectures Series 3
Optical (reduced) mass m
Watch the signs for inverted semiconductors.
Fox, Chapter 3
3
Optical mass follows from crystal momentum conservation.

## Slide 31: Intravalence Band Transitions
Braunstein & Kane, JPCS 1962
Braunstein, JCPS 1959
AlSb
D0
Kaiser, Phys. Rev. 91, 1380 (1953).
Kahn, Phys. Rev. 97, 1647 (1955).
D0
Eind
D0
p-type semiconductors
Also in gapless semiconductors
Ge
III/V
Stefan Zollner, 2023

## Slide 32: Carrier Concentration versus Temperature in a-Sn
Electrical Hall measurements are common to determine the dependence of the carrier concentration on temperature.
C.A. Hoffman, PRB 40, 11693 (1989).
n=p=4×1018 cm-3
Stefan Zollner, 2023

## Slide 33: Intravalence Band Transitions in a-Sn
Stefan Zollner, 2023
R.A. Carrasco, APL 113, 232104 (2018).
All gapless (inverted) semiconductors should have this peak.
Theory calculated with same model as for Ge.
Theory
Experiment

## Slide 34
Stefan Zollner, 2023
R.A. Carrasco, APL 113, 232104 (2018).
Note the negative sign in the optical mass.
Mid-IR absorption peak due to IVB transitions.
Optical mass m
EF
Theory
Experiment
All gapless semiconductors should have this peak. Theory calculated with same model as for Ge.
Intravalence Band Transitions in a-Sn

## Slide 35: Dependence on Temperature: No shift ???
Stefan Zollner, 2023, AFRL Lectures Series 3
R.A. Carrasco, APL 113, 232104 (2018).
Optical mass m
EF
Theory needs to address: Fermi-Dirac statistics (not important).
Nonparabolic bands (Kane’s k·p model).
k-dependent matrix elements (Kane).
Excitons (Tanguy) – not important.
Screening of excitons (Tanguy) – not important.
Theory
Experiment

## Slide 36: Doping with Germanium: Sn1-xGex alloys
Stefan Zollner, 2023
No significant change when doping a-Sn with up to 6% Ge.
R.A. Carrasco, APL 113, 232104 (2018).

## Slide 37: Dependence on Substrate (InSb or CdTe)
Stefan Zollner, 2023
R.A. Carrasco, APL 113, 232104 (2018).
Red: InSb substrate
Green: CdTe substrate
The intravalence band peak in a-tin is visible on both InSb and CdTe substrates.
Linear background is different (probably doping, Drude term). Depolarization is a problem for DSP substrates.

## Slide 38: Condensation of excitons at high density
Exciton gas
Electron-hole liquid
Mott transition (insulator-metal) when electron separation equals exciton radius.
Electron separation d for density N
Mott transition occurs at rs near 1.
GaAs: n=1017 cm-3.
Biexciton, triexciton molecule formation.
Electron-hole droplets. Bose-Einstein condensation.
dimensionless
Fox, Chapter 4
Stefan Zollner, 2023

## Slide 39: Excitons in doped or excited semiconductors
C. Tanguy, Phys. Rev. 60, 10660 (1999).
Banyai & Koch, Z. Phys. B 63, 283 (1986).
Need to include exciton screening due to doping.
Yukawa potential: Schrödinger equation not solvable.
Use Hulthen potential as an approximation
Coulomb
Yukawa
Hulthen
Hulthen exciton
Unscreened: g=∞
Fully screened: g=0
Mott criterion: g=1
Debye screening length
Stefan Zollner, 2023

## Slide 40: Tanguy: Dielectric function of screened excitons
C. Tanguy, Phys. Rev. B 60, 10660 (1999)
Bound exciton states (finite number):
exciton continuum:
Need to introduce Lorentzian broadening and perform numerical KK transform.
Reduced Rydberg energy
Stefan Zollner, 2023

## Slide 41: Tanguy: Dielectric function of screened excitons
Stefan Zollner, 2023
g=∞
g=0
g=0
g=∞
g=1.5
g=0
g=∞
C. Tanguy, Phys. Rev. B 60, 10660 (1999)
Small Broadening
Large Broadening
g=∞
g=0

## Slide 42: Excitons in laser-excited GaAs
GaAs 300 K
High laser excitation
g=∞
g small
Haug and Koch, Quantum Theory of Optical and Electronic Properties of Semiconductors
Y. H. Lee, Phys. Rev. Lett 57, 2446 (1986)
Hulthen exciton
Stefan Zollner, 2023

## Slide 43: Excitons in doped or excited semiconductors
High laser excitation
High doping
Fox, Chapter 4
Fujiwara, Phys. Rev. B 71, 075109 (2005)
Exciton peak broadens
Stefan Zollner, 2023

## Slide 44: Thermal ionization of excitons in Germanium
E0
E0+Δ0
10 K
718 K
Strong excitonic peak at 10 K, disappears at high T.
Excitonic (Sommerfeld) enhancement persists at high temperatures.
Ge
EX(hh)=1.7 meV
kB=0.086 meV/K
TC=20 K
Stefan Zollner, 2023

## Slide 45: Dielectric function of InSb from 80 to 800 K
Stefan Zollner, 2023
Rivero Arias, JVSTB 41, 022203 (2023)
Band gap changes with temperature (but only below 500 K).
Amplitude reduction at high temperatures (Pauli blocking, bleaching)
Drude response at high temperatures (thermally excited carriers).
Depolarization artifacts at long wavelengths (below 300 K).
Woollam FTIR-VASE
cryostat with CVD diamond windows
InSb
InSb
Kane, J. Phys. Chem. Solids 1, 249 (1957). Kane 1966.

## Slide 46: Temperature Dependence of InSb
Stefan Zollner, 2023, AFRL Lectures Series 3
InSb
Parametric-Semiconductor (PSEMI) Model:
Also vary “shape parameters”.
Asymmetric peak shape poorly described.
Try Tanguy oscillator for excitonic line shape.
How does the dielectric function of InSb near the band gap change with temperature?
C. M. Herzinger, B. Johs, et al., J. Appl. Phys. 83, 3323 (1998).
Rivero Arias, JVST B 41, 022203 (2023).

## Slide 47: Burstein-Moss Shift
Stefan Zollner, 2023, AFRL Lectures Series 3
Bose-Einstein Model
]
Band gap changes with temperature (but only below 500 K)
Described by Bose-Einstein model below 500 K: Logothetidis, PRB 31, 947 (1985).
No redshift above 500 K: Thermal Burstein-Moss shift
InSb
T.S. Moss, Proc. Phys. Soc. 67, 775 (1954).
E. Burstein, Phys. Rev. 93, 632 (1954).

## Slide 48: Fermi Level versus Temperature in Intrinsic InSb
kBT=Eg/4 at 600 K
Fermi level above the conduction band edge above 450 K.
(Calculated for constant m and Eg).
Need to include nonparabolicity.
InSb
(simple model)
n=4x1017 cm-3 at 800 K
Thermal Burstein-Moss shift
Drude response of free carriers
Reduction of absorption coefficient
Calculated for constant mass and band gap.
Rivero Arias, JVSTB 41, 022203 (2023)
Kane, J. Phys. Chem. Solids 1, 249 (1957). Kane 1966.
Stefan Zollner, 2023

## Slide 49: Carrier concentration and mobility from 80 to 800 K
Stefan Zollner, 2023, AFRL Lectures Series 3
To model the Drude response, we make some really simple assumptions:
Parabolic bands (ignore non-parabolicity)
Effective mass constant me=0.014 (independent of temperature)
Oswaldowski/Zimpel, J. Phys. Chem. Solids 49, 1179 (1988).
D. L. Rode, Phys. Rev. B 3, 3287 (1971).
Carrier concentration
of InSb
Reasonable agreement with Hall measurements.
Large errors below 400 K (depolarization).
Drude mobility of InSb

## Slide 50: Required improvements: Screened Excitons
Stefan Zollner, 2023, AFRL Lectures Series 3
Absorption by screened excitons (Hulthen potential): Better lineshape.
Numerical Kramers-Kronig transform (Tanguy cannot be used due to fh, fe ≠0).
Degenerate Fermi-Dirac statistics to calculate fh and fe.
Two terms for light and heavy excitons
Non-parabolicity and temperature-dependent mass included from k.p theory
k-dependent matrix element P.
Screening parameter g=12/p2aRkTF (large: no screening)
Only two free parameters: Band gap E0 and broadening G.
Amplitude A and exciton binding energy R from k.p theory and effective masses.
Christian Tanguy, Phys. Rev. B 60, 10660 (1999).
Jose Menendez, Phys. Rev. B 101, 195204 (2020).
Carola Emminger, J. Appl. Phys. 131, 165701 (2022).
This theory needs to be used for InSb, a-tin, Ge-Sn alloys.

## Slide 51: Germanium-Tin Alloys
Stefan Zollner, 2023

## Slide 52: Germanium-Tin Alloys
Stefan Zollner, 2023
M.P. Polak, J. Phys. D 50, 195103 (2017).
DFT calculation (GGA, WIEN2k, 54-atom supercell)
indirect (Ge)
direct (GaAs)
inverted (Sn)
inverse SO
topological insulators

## Slide 53: Germanium-Tin Alloys
Stefan Zollner, 2023
M.P. Polak, J. Phys. D 50, 195103 (2017).
These alloys are a rich playground to explore the various topological phases available in common semiconductors.
This DFT calculation (GGA, WIEN2k, 54-atom supercell) does not agree so well with experiments.
Synthesis of alloys over the complete range of compositions and measurements of the band gaps are needed.

## Slide 54: Award-winning undergraduate research students
54
Stefan Zollner, 2023

## Slide 55: Intravalence Band Transitions in Topological Insulators
Bonds and Bands
Band Structure of Silicon, Germanium, and a-Tin
Why is a-Tin a Topological Insulator?
Intravalence Band Absorption in Ge and AlSb
Intravalence Band Absorption in a-Tin
Dependence on Temperature, Substrate, and Doping with Ge
Summary
Stefan Zollner, 2023
Woollam FTIR-VASE;
cryostat with CVD diamond windows

## Slide 56: Thank you! Questions?
AVS 2022, Pittsburgh, PA

## Slide 57: Ellipsometry Measurement
Stefan Zollner, 2023, AFRL Lectures Series 1
Fresnel reflection ratio
Polarization State
Jones Vector
Ellipsometry Experiment
Fresnel reflection coefficients
Isotropic surface:
Off-diagonal elements vanish.
Anisotropy or depolarization (not both)

## Slide 58: Experimental Methods
Spectroscopic Ellipsometer 190 to 2500 nm (0.5 to 6.5 eV)
Spectroscopic Ellipsometry:
Thickness (100 to 10000 Å)
Absorption, band gap
Refractive index
detector
Monochromator
polarizer
sample
analyzer
Φ
X-ray diffraction & reflectance
XRD/XRR:
Crystal structure
Lattice spacings (strain)
Thickness (5 Å to 1000 Å)
Surface, roughness layer
Density
Infrared Ellipsometer 1.25 to 40 mm (250 to 8000 cm-1)
FTIR ellipsometry:
Very thick films (> 5000 Å)
Phonon absorption
Optical Constants
Notes: Birstein-Moss shift

## Slide 59: Ellipsometry from 190 nm to 40,000 nm
Two different instruments are used for measurements from the mid-infrared to the deep ultraviolet spectral range.
J.A. Woollam IR-VASE
SZ, Spectroscopic Ellipsometry from 10 to 700 K, Adv. Opt. Technol. 11, 117 (2022).
J.A. Woollam V-VASE

## Slide 60: Temperature-dependent ellipsometry: 10-700 K
Using FTIR spectroscopic ellipsometry in an ultra-high vacuum (UHV) cryostat with CVD diamond windows (Janis ST-400, Diamond Materials GmbH, Freiburg).
Why diamond? Large transparency range and good vacuum seals, but expensive and high reflection losses.
J.A. Woollam IR-VASE
Energies: 30-40 meV to 1 eV
VIS-UV and FTIR spectra (dielectric functions) After oxide correction (25 Å)
Cryostat with CVD diamond windows
E0
Compare:
Aspnes, PRB 27, 985 (1983)
Logothetidis, PRB 31, 947 (1985).
Schaefer, JAP 127, 165705 (2020).
SZ, Adv. Opt. Technol. 11, 117 (2022).
InSb

## Slide 61: Free-Electron Approximation with Effective Masses
Stefan Zollner, 2023, AFRL Lectures Series 3
Ignore potential energy (V=0)
Effective mass m*
Free particle: Plane wave
Effective mass tensor
Yu & Cardona, Fundamentals of Semiconductors
Ge

## Slide 62: k·p Theory (Band Structure Method)
Stefan Zollner, 2023, AFRL Lectures Series 3
Schrödinger equation
Use Bloch’s theorem:
Solve equation for k=0.
Eliminate green free-electron term with substitution of variables (Kane 1957).
Then treat red term in perturbation theory.
Works very well for semiconductors with local V(r) potentials.
Yu & Cardona, Fundamentals of Semiconductors
Kane, J. Phys. Chem. Solids 1, 249 (1957). Kane 1966.
Product rule

## Slide 63: k·p Theory: Effective Mass of Non-Degenerate Band
Stefan Zollner, 2023, AFRL Lectures Series 3
Yu & Cardona, Fundamentals of Semiconductors
Solve for k=0 (at G). Linear terms in k vanish (extremum).
Treat red term in perturbation theory (up to second order).
Effective mass comes from band-band interactions.
The same k·p momentum matrix element determines the strength of interband transitions.

## Slide 64: k·p Theory: Application to Electron Band at G
Stefan Zollner, 2023, AFRL Lectures Series 3
Keep only the largest term:
Momentum matrix element:
EP=2P2/m0
EP≈20 eV
64
Stefan Zollner, 2023, AFRL Lectures Series 3
Yu & Cardona, Fundamentals of Semiconductors