## Slide 1: Impact of Stress and Strain on Optical Spectra of Semiconductors
Stefan Zollner
Department of Physics
New Mexico State University Las Cruces, NM, USA
FA9550-20-1-0135
W911NF-2210130
Email: zollner@nmsu.edu. WWW: http://femto.nmsu.edu.
Ask me about MS/Ph.D. student positions at NMSU..

## Slide 2
Biography
Regensburg/Stuttgart
Germany
Las Cruces, NM
Since 2010
Motorola (Mesa, Tempe)
Arizona, 1997-2005
Motorola, Freescale
Texas, 2005-2007
Freescale, IBM
New York, 91-92;07-10

## Slide 3: Where is Las Cruces, NM ???
White Sands NP

## Slide 4: Finally in Grenoble
STM fab in Crolles
Dès 1972, une collaboration est engagée entre le SNCI et le Max-Plank-Institut für Festkörperforschung (MPI-FKF) de Stuttgart (avec Dransfeld). La puissance est portée à 10 MW en 1974, ce qui permet d’atteindre en 1982 des champs de 25T dans un diamètre de 50 mm, avec les premières polyhélices construites par Hans Schneider-Muntau. C’est dans les champs intenses de Grenoble que Klaus von Klitzing découvre l’effet Hall quantique entier dans la nuit du 4 au 5 février 1980, qui lui vaut le prix Nobel de physique en 1985.
Dr. Maria Spies
Universite Grenoble Alpes
Now a physics postdoc in Pisa.

## Slide 5: Outline: tutorial on stress and strain
Hooke’s Law
Stress and strain tensors
Elasticity and compliance tensors
Examples of stress along one, two, and three directions
Strain measurements using high-resolution x-ray diffraction
Impact of strain on phonon energies (Raman spectra)
Impact of strain on band energies with CMOS applications
Impact of strain on optical spectra of semiconductors
Example: Pseudomorphic Ge-Sn alloy layer on GaAs
Stefan Zollner, 2023, Grenoble

## Slide 6: Hooke’s Law
Stefan Zollner, 2023, Grenoble
Young & Freedman, University Physics.
In one dimension, the stress is the force (measured in N).
The strain is the relative length change (dimensionless).
k is the spring constant (elasticity constant).
Let’s rewrite this:
r Length of unstretched spring (m)
r’ Length of stretched spring (m)
u=r’-r Displacement of spring (m)
e=u/r Strain (relative displacement), dimensionless
c=kr Elasticity constant (N)
F=ce Hooke’s Law in one dimension

## Slide 7: Stress tensor
Landau-Lifshitz, Vol. 7, Elasticity Theory.
Wikipedia
Stress defined as force per unit area.
Measured in units of MPa or GPa.
Sum of all forces (net force) must be zero.
Forces show inversion symmetry at opposite faces of the cell.
Net torque must be zero: Stress tensor symmetric.

## Slide 8: Examples of stress tensors
Landau-Lifshitz, Vol. 7, Elasticity Theory.
Google images
Hydrostatic pressure
Uniaxial stress
Biaxial stress
Diamond anvil cell
Thin rod in a vise
Strained Si
Relaxed SiGe
Relaxed SiGe
Relaxed Si
Pseudomorphic epitaxial layer

## Slide 9: Measurement of wafer curvature (stress)
Wikipedia
Measurement of stress with x-rays
k-Space Associates, Inc.
Flexus 2320-S
Dektak XT (stylus)
Stoney’s Equation:

## Slide 10: Strain tensor
Landau-Lifshitz, Vol. 7, Elasticity Theory.
r Position of the unstrained point
r’ Position of the strained point
u(r)=r’-r Displacement (vector field)
The strain tensor e(r) is defined by
u(r)=e(r)r
This is a tensor field.
We assume a homogeneous strain e(r)=e.
Volume change: DV/V=Tr(e)
Poisson ratio: (0<n<0.5)
Sign convention: Positive e: Tensile strain
Negative e: Compressive strain
Onsager principle:
The strain tensor is symmetric. It can be diagonalized (principal axes).
Determinant usually non-zero (Poisson ratio).

## Slide 11: Examples of strain tensors
P.Y. Yu and M. Cardona, Fundamentals of Semiconductors.
Hydrostatic strain
(001) uniaxial shear strain
(111) uniaxial shear strain
Group theory: An arbitrary strain has a unique decomposition into a hydrostatic and (100) and (111) pure shear components.
Traceless: No volume change
Pressure P
Bulk modulus B (GPa)
In practical experimental geometries (uniaxial or biaxial stress) we usually find both hydrostatic and uniaxial shear components.

## Slide 12: Strain measurements
Ge1-ySny on GaAs (y=2.6%)
Asymmetric (224) grazing incidence reciprocal space map (XRD)
Transmission electron microscopy:
Selected area diffraction
Atom probe tomography
Stefan Zollner, 2023, Grenoble

## Slide 13: Elasticity and compliance tensors (Hooke’s Law)
Elasticity (stiffness) tensor cijkl
Compliance tensor Sijkl
These are fourth rank-tensors with 81 elements.
Stress and strain tensors are symmetric, therefore only 21 elements are needed for c and S.
No factors of 2,4 for cij.
i,j=1..6
i,j=1..6
k,l=1..3
Landau-Lifshitz, Vol. 7, Elasticity Theory.
6x6 matrices are symmetric: 21 elements

## Slide 14: Compliance tensors for different symmetries
Nye, Physical Properties of Crystals, Appendix E.
The number of independent elements of the compliance tensor is reduced further by crystal symmetry.
Triclinic system: 21 elements
Cubic system: We only have three elements: s11, s12, s44
Cubic point groups

## Slide 15: Phonon spectra under uniaxial strain
Uniaxial strain splits the three-fold degenerate Raman phonon in Si into a singlet and a triplet.
For this strain tensor, the stress could be uniaxial or biaxial along (100).
R. Liu and N. Cave in Pantelides and Zollner: Silicon-Germanium-Carbon Alloys.
Silicon (001)
Only the singlet is observable in conventional backscattering geometry.

## Slide 16: UV Raman stress mapping in Si devices
325 nm He-Cd laser, 0.4 mm spot size
UV-enhanced spectrometer
Useful for devices with half-pitch greater than 0.13 mm
Obsolete since around 2002.
R. Liu, Freescale Semiconductor
90nm node

## Slide 17: UV Raman stress measurements in group-IV alloys
Jean-Michel Hartmann, CEA-LETI, Grenoble
Raman spectroscopy is useful to determine the composition of Si-Ge-Tin alloys, but strain must be subtracted in the analysis.

## Slide 18: Electronic bands under hydrostatic strain
Valence bands remain about the same.
(Deformation potential aV is small.)
Conduction bands:
G-point moves up fast (aC=-10 eV).
L-point also moves up (Ge becomes more indirect).
X-point moves down (GaAs becomes indirect at 41 kbar).
Paul’s rule: Deformation potentials do not vary much between semiconductor materials for the same band or transition.
Stefan Zollner, 2023, Grenoble
Deformation potential:

## Slide 19: Valence bands of Si under (001) stress
A uniaxial compressive stress is created by embedded Si-Ge source-drain stressors.
Under compressive uniaxial stress, the hole mobility increases.
This technology is used for most high-performance PMOS transistors.
Pantelides and Zollner, Silicon-Germanium-Carbon Alloys.

## Slide 20: Conduction bands of Si under (001) stress
A uniaxial compressive stress splits the six-fold degenerate conduction band valleys of Si.
This reduces the f- and g-intervalley scattering and also changes the effective masses.
This can be achieved with tensile nitride stress liners or with embedded Si-C alloy stressors.
Pantelides and Zollner, Silicon-Germanium-Carbon Alloys.

## Slide 21: Photoluminescence of Si1-xGex alloys on Si
Pantelides and Zollner, Silicon-Germanium-Carbon Alloys.
Pseudomorphic growth of Si1-xGex alloy on Si (001)

## Slide 22: Strain splitting of E1 and E1+D1 transitions
Large shear approximation (small spin-orbit splitting)
Small shear approximation (large spin-orbit splitting)
E1
Pantelides and Zollner, Silicon-Germanium-Carbon Alloys.

## Slide 23: Spectroscopic ellipsometry
femto.nmsu.edu
UHV cryostat
& V-VASE ellipsometer

## Slide 24: Ellipsometry instrumentation
femto.nmsu.edu
UHV cryostat
& V-VASE ellipsometer
Broadband versus scanning monochromator
FTIR and near-IR/VIS/near-UV
Compensator is crucial for small D
Dual rotating compensators: Full Mueller matrix
Option: Phase-modulation ellipsometry
Equidistant energies or wavelengths
Spot size: 10 mm or 30 mm on 1 mm (imaging)
Stefan Zollner, 2023, Grenoble

## Slide 25: Penetration depth
The penetration depth is the inverse of the absorption coefficient, which can be measured with spectroscopic ellipsometry.
Below the direct band gap (0.8 eV for Ge, 3.4 eV for Si), the penetration depth is very large (many microns).
The penetration depth is smallest at the E2 peak in the UV, about 10 nm.

## Slide 26: Critical points in the dielectric function of Ge
Structures in the dielectric function
Due to interband transitions
P.Y. Yu and M. Cardona, Fundamentals of Semiconductors.

## Slide 27: Piezo-optics of Si, Ge, GaAs under (001) strain
Elasto-optical constants of Si
P. Etchegoin, J. Kircher, and M. Cardona
Phys. Rev. B 47, 10292 (1993).
Piezo-optics of GaAs
P. Etchegoin, J. Kircher, M. Cardona, C. Grein, and E. Bustarret
Phys. Rev. B 46, 15139 (1992).
Piezo-optical response of Ge in the visible–uv range
P. Etchegoin, J. Kircher, M. Cardona, and C. Grein
Phys. Rev. B 45, 11721 (1992).
Piezo-optics of InP in the visible-ultraviolet range
D. Rönnow, P. Santos, M. Cardona, E. Anastassakis, and M. Kuball
Phys. Rev. B 57, 4432 (1998: E: 1999).
Etienne Bustarret

## Slide 28: Tensile biaxial stress in Ge layers on Si
1 meV accuracy for E1 energy measurement.
Stefan Zollner, 2023, Grenoble

## Slide 29: Optical and X-Ray Characterization of Ge1-ySny alloys on GaAs
This work was supported by Air Force Office of Scientific Research under award number FA9550-20-1-0135.
Haley B. Woolf,1 Matt Kim,2 Carola Emminger,1
Carlos A. Armenta,1 Stefan Zollner1
Department of Physics, New Mexico State University, Las Cruces, NM, USA
QuantTera, Scottsdale, AZ, USA
2022 AVS International Symposium,
Pittsburgh, PA, USA. November 2023.
29

## Slide 30: Outline
Introduction
X-ray diffraction data:
  Omega scans (rocking curves), and reciprocal space maps on (004), (224), & reflections
Composition and lattice constant
Optical data:
  Pseudodielectric function, optical constants, and second derivative spectra
  Photoluminescence data: dependence of E0 on tin content
Dependence of E1 and E1+Δ1 on tin content (ellipsometry)
Conclusion
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
30

## Slide 31: Introduction
GeSn alloys with tunable bandgaps are of interest for mid infrared lasers and detectors. They can be integrated with common semiconductor substrates (Si, Ge, GaAs).
Two Ge1-ySny layers were grown on GaAs by chemical vapor epitaxy with different amounts of tin. The tin content is found with (004) omega rocking curves and reciprocal space maps.
The tin contents were found to be 1.2% and 2.6% with thicknesses of 1600 Å and 1150 Å, respectively.
Asymmetric grazing incidence and grazing exit reciprocal space maps were used to determine the strain and relaxation of the epitaxial layer.
From the dielectric function and the tin content, we can compare the E1 and E1+Δ1 energies with continuum elasticity theory. When the tin content increases, the energies decrease.
Photoluminescence data was taken of both samples and compared to bulk Ge to observe the change in E0. Using continuum elasticity theory for E0, we see that when the tin content increases, the energies decrease.
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
31

## Slide 32: (004) Rocking Curves: Strained or relaxed ???
ω Scan Open Detector:
ω-2θ Scan Open Detector:
FWHM
GaAs 0.010°
GeSn 0.016°
GaAs 0.010°
GeSn 0.017°
Bulk GaAs 0.0077°
Bulk Ge 0.0074°
Vertical Lattice Constants:
GaAs: 5.652 Å
GeSn: 5.679 Å
GaAs: 5.652 Å
GeSn: 5.699 Å
Bulk GaAs: 5.653 Å
Bulk Ge: 5.658 Å
Taken at 2θ = 66.4240°
FWHM
GaAs 0.010°
GeSn 0.016°
GaAs 0.010°
GeSn 0.017°
Bulk GaAs 0.0078°
Bulk Ge 0.0074°
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
32
Even the GaAs substrate is broader if an epilayer has been grown (dislocations may penetrate from the epilayer into the substrate).
Notes: 004 is symmetric scan. Using braggs law and the angle of reflection we can find the d-spacings of the samples. The epitaxial layer on the receiving slit graph are missing because of the width of the detector.

## Slide 33: (004) Reciprocal Space Maps
Dashed line drawn through substrate peak
M-Mosaic Spread (Relaxation Line)
GeSn on GaAs 2.6%
Bulk GaAs
Bulk Ge
GeSn on GaAs 1.2%
33
No tilt between epilayer and substrate.

## Slide 34: & Rocking Curve (Open Detector)
() Grazing Exit
(224) Grazing Incidence
FWHM
GaAs: 0.017°
GeSn: 0.022°
GaAs: 0.013°
GeSn: 0.013°
Bulk GaAs: 0.011°
Bulk Ge: 0.011°
FWHM
GaAs: 0.022°
GeSn: 0.028°
GaAs: 0.033°
GeSn: 0.041°
Bulk GaAs: 0.013°
Bulk Ge: 0.015°
X-ray tube
Detector
X-ray tube
Detector
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
34
Notes: 224 RSM are asymmetrical scans using xrd. Since delta omega on both sides are not equal, this tells us that the samples are not fully relaxed.

## Slide 35: (224) Grazing Incidence RSM
GaAs
GeSn
W-Wavelength Streak
M-Mosaic Spread (Relaxation Line)
Black line drawn from origin (Relaxed)
Dashed line drawn through substrate peak (Pseudomorphic)
Bulk GaAs
Bulk Ge
GeSn on GaAs 1.2%
GeSn on GaAs 2.6%
35

## Slide 36: Lattice Constants
|| substrate= 5.653 Å
Poisson Ratio:
GeSn= 5.679 Å Sn= 6.489 Å
GeSn= 5.699 Å Ge= 5.658 Å
GaAs = 5.653 Å
Vegard’s Law:
If layers is fully relaxed, the % Sn is 2.6% and 5.0%
If layers is fully strained, the % Sn is 1.2% and 2.6%
Bragg’s Law:
(Pseudomorphic Condition)
Lattice Constants:
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
36
Notes: With Vegard’s law and continuum elasticity theory, the tin content of the Ge1-ySny layer can be found with the measured and known lattice constants of GaAs, Ge, and Sn.

## Slide 37: Pseudodielectric function before/after cleaning: 1.2%
The Ge1-ySny on GaAs sample was cleaned ultrasonically with water and then isopropanol for 15 mins each to remove organic layers and most of the native oxide.
 | Oxide Thickness
As Received (May 20th): | 43.66 Å
Before Cleaning (June 14th): | 72.07 Å
After Cleaning (June 14th): | 26.50 Å
After 2nd Cleaning (June 15th): | 25.90 Å
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
37

## Slide 38: Pseudodielectric Function
GeSn on GaAs 1.2%
GeSn on GaAs 2.6%
GaAs
Ge1-ySny
Oxide
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
38

## Slide 39: Ge1-ySny optical constants
GaAs
Ge1-ySny
Oxide
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
39

## Slide 40: 2nd Derivative of the dielectric Function: 2.6% tin
Critical Points of Ge (Orange)
Critical Points of GeSn 2.6% (Blue)
CP | E (eV) | A | Φ (deg) | Γ (meV) | n
E1 | 2.113 | 5.32 | 246 | 0.050 | 0
E1+Δ1 | 2.314 | 3.53 | 246 | 0.066 | 0
E’0 | 3.099 | 1.33 | 175 | 0.102 | 0
E’0+Δ’0 | 3.344 | 0.486 | 266 | 0.139 | 0
E2 | 4.354 | 11.2 | 318 | 0.097 | 0
CP | E (eV) | A | Φ (deg) | Γ (meV) | n
E1 | 2.066 | 6.701 | 225.0 | 0.0769 | 0
E1+Δ1 | 2.285 | 2.958 | 225.0 | 0.0862 | 0
E’0 | 3.138 | 2.669 | 314.9 | 0.2027 | 0
E’0+Δ’0 | 3.299 | 0.060 | 189.3 | 0.0485 | 0
E2 | 4.339 | 10.72 | 232.9 | 0.1148 | 0
40
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
Notes: By fitting the 2nd derivative of the dielectric function, the critical point parameters were found. This includes energy, amplitude, phase angle, broadening, and the line shape. The phase angle for E1 and E1+Δ1 were fixed to be the same.

## Slide 41: Dependence of E1 & E1+Δ1 energies on tin content
Relaxed:
Strained:
eV,
eV,
eV,
eV,
small shear approximation
41
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.
Notes: The marked squares are the measured energies of bulk Ge and the Ge1-ySny epitaxial layer. The Ge1-ySny energy for the E1 is slightly higher.

## Slide 42: Photoluminescence spectra of Ge-Sn alloys at 300K
Indirect Direct
Bandgap (eV) Bandgap (eV)
Bulk Ge: 0.679 0.772
GeSn (1.2%): 0.657 0.748
GeSn (2.6%): 0.651 0.705
42
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.

## Slide 43: Dependence of direct bandgap E0 on tin content
eV,
eV,
eV,
eV,
A
B
Strained:
Relaxed:
43
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.

## Slide 44: Conclusion
The (224) reciprocal space maps showed that the GeSn epitaxial layer was grown pseudomorphically on both samples.
Using Vegard’s Law, continuum elasticity theory, and the (004) reciprocal space map, the tin content is found to be y=0.012 and y=0.026.
After cleaning the sample, the thickness of the oxide was reduced to 26 Å and 23 Å.
Using the ellipsometry data, the fitted GeSn dielectric function was similar to bulk Ge most likely because of the low tin content.
The fit second derivative of the dielectric function helped find the critical point parameters and compared to bulk Ge.
44
Haley B. Woolf et al., 2022 AVS Symposium,
Pittsburgh, PA, USA. November 2023.

## Slide 45: Conclusions
Hooke’s Law
Stress and strain tensors
Elasticity and compliance tensors
Examples of stress along one, two, and three directions
Strain measurements using high-resolution x-ray diffraction
Impact of strain on phonon energies (Raman spectra)
Impact of strain on band energies with CMOS applications
Impact of strain on optical spectra of semiconductors
Example: Germanium-tin alloys grown pseudomorphically on GaAs
Stefan Zollner, 2023, Grenoble
Notes: Birstein-Moss shift

## Slide 46: Thank you! Questions?

## Slide 47: New slide