## Slide 1: Spectroscopic Ellipsometry Studies of Optical Constants in Highly Excited Semiconductors
Stefan Zollner
With: Carola Emminger, Jose Menendez, Carlos A. Armenta, Melissa Rivero Arias, Jaden R. Love, Cesy M. Zamarripa, Sonam Yadav, Shirly Espinoza, Mateusz Rebarz, Martin Zahradnik, Jakob Andreasson
College of Arts and Sciences, Department of Physics
New Mexico State University, Las Cruces, NM, USA
Sonderkolloquium TU Ilmenau, 24.3.2023
FA9550-20-1-0135
W911NF-2210130
Email: zollner@nmsu.edu. WWW: http://femto.nmsu.edu.
Ask me about MS/Ph.D. student positions at NMSU..
AVS 2022, Pittsburgh, PA

## Slide 2
Biography
Regensburg/Stuttgart
Germany
Las Cruces, NM
Since 2010
Motorola (Mesa, Tempe)
Arizona, 1997-2005
Motorola, Freescale
Texas, 2005-2007
Freescale, IBM
New York, 91-92;07-10

## Slide 3: Where is Las Cruces, NM ???
White Sands NP

## Slide 4: Problem Statement
(1) Achieve a quantitative understanding of absorption and emission processes.
Our qualitative understanding of such processes is 50-100 years old,
But insufficient for modeling of detectors and emitters.
(2) How are optical processes affected by high carrier concentrations (screening)?
High carrier densities can be achieved with
  In situ doping or
  ultrafast lasers or
  high temperatures.
Goal: CMOS-integrated mid-infrared camera (thermal imaging with a phone).
Future: How are optical processes affected by an electric field (pin diode or thin layer)?

## Slide 5
5

## Slide 6: Example 1: Photoluminescence in Germanium
Menendez, Poweleit, Tilton, PRB 101, 195204 (2020).
Qualitative:
Quantitative:
Roosbroeck-Shockley equation (PR 94, 1558, 1954).
Complete failure above 200 K and at RT.

## Slide 7: Example 2: Indirect Absorption in Germanium
R. J. Elliott, Phys. Rev. 108, 1384 (1957).
Menendez, Lockwood, Zwinkels, Noel, PRB 98, 165207 (2018).

## Slide 8: Optical Constants of Highly Excited Semiconductors
Einstein coefficients, Fermi’s Golden Rule, Elliott-Tanguy excitons
Direct gap absorption in germanium from 10 to 800 K
Optical constants of highly excited semiconductors
  Direct gap absorption in InSb from 10 to 800 K
  Optical constants of highly excited germanium (femtosecond ellipsometry at ELI Beamlines in Prague)
Conclusion and Outlook

## Slide 9: Einstein Coefficients
Albert Einstein, Strahlungs-Emission und Absorption nach der Quantentheorie, DPG Verh. 18, 318 (1916); Phys. Z. 18, 121 (1917).
A21
B12
B21
In equilibrium: N1, N2 constant. Absorption and emission balance.
Black-body radiation
One coefficient is sufficient:
Use Fermi’s Golden Rule to calculate B12

## Slide 10: Fermi’s Golden Rule: Tauc Plot
Direct band gap absorption
Use k·p matrix element P: EP=2P2/m0
Fox, Chapter 3
constant k·p matrix element
Joint DOS

## Slide 11: Fermi’s Golden Rule: Tauc Plot
Direct band gap absorption
Use k·p matrix element P: EP=2P2/m0
The Tauc plot is wishful thinking.
No linear region:
Broadening.
1/E2 denominator.
excitons
Melissa Rivero Arias

## Slide 12: Practical Tip: Oxide or Surface Correction
Below the band gap, e2 must be exactly zero for a bulk insulator (not positive, not negative).
This method requires a compensator to measure D exactly near 0 or 180 degrees.
(Also change JAW software settings to allow negative e2 values.)
G.E. Jellison and B.C. Sales, Determination of the optical functions of transparent glasses by using spectroscopic ellipsometry, Appl. Opt. 30, 4310 (1991).
Optical constants for anodic oxide of InSb:
e∞3.8
Mattausch, PRB 23, 1896 (1981).
Zollner, APL 63, 2523 (1993).
Jellison-Sales Method for Transparent Glasses: How thick is the surface region?
InSb

## Slide 13: Elliott-Tanguy Exciton Absorption
Direct band gap absorption
Excitonic binding energy: R=RH×mh/es2
´
bound excitons
exciton continuum enhancement
Tanguy’s contributions:
Add Lorentzian broadening
Kramers-Kronig transform to get the real part.
R. J. Elliott, Phys. Rev. 108, 1384 (1957).
Christian Tanguy, Phys. Rev. Lett. 75, 4090 (1995) + (E)

## Slide 14: Calculation of Absorption Spectrum from k.p Theory
Can we calculate the absorption spectrum?
Yes, we can for Ge in the low carrier density limit.
It does not work for other III/V compounds.
How can we calculate the absorption for high carrier densities?
Carola Emminger et al., JAP 131, 165701 (2022).

## Slide 15: Elliott-Tanguy theory applied to Ge
ε1
ε2
Fixed parameters:
  Electron and hole masses (temperature dependent)
  Excitonic binding energy R
  Amplitude A (derived from matrix element P)
Adjustable parameters:
  Broadening Γ: 2.3 meV
  Band gap E0
  Linear background A1 and B1 (contribution from E1 to real part of e)
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
15
Quantitative agreement

## Slide 16: Elliott-Tanguy theory applied to Ge
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
??? at high T.
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
16

## Slide 17: Elliott-Tanguy theory: Problems for Ge at high T
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
??? at high T.
Measurement error ??
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
17

## Slide 18: Optical Absorption at High Carrier Densities
Intense femtosecond laser excitation (ELI Beamlines) (electrons pile at L-point)
High n-doping of Ge with P
(free electrons pile up at L-point)
Xu et al., PRL 118, 267402 (2017)
High temperature
(thermal excitation of e-h pairs)
constant m and Eg
InSb
Rivero, JVSTB 41, 022203 (2023)
Espinoza, APL 115, 052105 (2019)
18

## Slide 19: (1) Dielectric function of InSb from 80 to 800 K
Rivero Arias, JVSTB 41, 022203 (2023)
19
Band gap changes with temperature (but only below 500 K).
Amplitude reduction at high temperatures (Pauli blocking, bleaching)
Drude response at high temperatures (thermally excited carriers).
Depolarization artifacts at long wavelengths (below 300 K).
Woollam FTIR-VASE
cryostat with CVD diamond windows
InSb
InSb

## Slide 20: Band gap analysis for InSb
C. M. Herzinger, B. Johs, et al., J. Appl. Phys. 83, 3323 (1998)
Rivero Arias, JVSTB 41, 022203 (2023)
20
How does the band gap of InSb change with temperature?
Parametric-Semiconductor Model:
Also vary “shape parameters”.
Asymmetric peak shape poorly described.
Try Tanguy oscillator for excitonic line shape.
InSb

## Slide 21: Band gap of InSb from 80 to 800 K
21
Bose-Einstein Model
]
Band gap changes with temperature (but only below 500 K)
Described by Bose-Einstein model below 500 K: Logothetidis, PRB 31, 947 (1985).
No redshift above 500 K: Thermal Burstein-Moss shift
T.S. Moss, Proc. Phys. Soc. 67, 775 (1954).
E. Burstein, Phys. Rev. 93, 632 (1954).
InSb

## Slide 22: Thermal excitations of electron-hole pairs in InSb
kBT=Eg/4 at 600 K
Fermi level above the conduction band edge above 450 K.
(Calculated for constant m and Eg)
Rivero Arias, JVSTB 41, 022203 (2023)
22
InSb
(simple model)
n=4x1017 cm-3 at 800 K
Thermal Burstein-Moss shift
Drude response of free carriers
Reduction of absorption coefficient
Calculated for constant mass and band gap.

## Slide 23: Carrier concentration and mobility from 80 to 800 K
23
To model the Drude response, we make some really simple assumptions:
Parabolic bands (ignore non-parabolicity)
Effective mass constant me=0.014 (independent of temperature)
Oswaldowski/Zimpel, J. Phys. Chem. Solids 49, 1179 (1988).
D. L. Rode, Phys. Rev. B 3, 3287 (1971).
Carrier concentration
of InSb
Reasonable agreement with Hall measurements.
Large errors below 400 K (depolarization).
Drude mobility of InSb

## Slide 24: Required model improvements: Screened Excitons
Absorption by screened excitons (Hulthen potential)
Kramers-Kronig transform following Tanguy (includes broadening G)
Degenerate Fermi-Dirac statistics to calculate fh and fe.
Two terms for light and heavy excitons
Non-parabolicity and temperature-dependent mass included from k.p theory
k-dependent matrix element P.
Screening parameter g=12/p2aRkTF (large: no screening)
Only two free parameters: Band gap E0 and broadening G
Amplitude A and exciton binding energy R from k.p theory and effective masses
Christian Tanguy, Phys. Rev. B 60, 10660 (1999).
Jose Menendez, Phys. Rev. B 101, 195204 (2020).
Carola Emminger, J. Appl. Phys. 131, 165701 (2022).

## Slide 25: (2) Highly doped Ge (n-type, with phosphorus)
Electrons pile up at the L-point.
Transitions in red region blocked.
Phase filling singularity
Xu et al., PRL 118, 267402 (2017)
Xu et al., JAP 125, 085704 (2019)
25
Phase shift

## Slide 26: (3) Set-up: Femtosecond pump-probe ellipsometry
Ch: Chopper (500 Hz, 250 Hz)
A: Analyzer
P: Polarizer
CR: Rotating compensator
L: Lens
S: Sample
DL: Delay Line (~6.67 ns pump-probe delay and 3 fs resolution)
BS: Beam splitter
SHG/THG: 2nd/3rd harmonic generation
SCG: Super-continuum generation
CCD: Charge-coupled device detector
26
Espinoza et al., APL 115, 052105 (2019).

## Slide 27: Set-up: Femtosecond pump-probe ellipsometry
27
Rotating compensator ellipsometer:
Compensator was rotated in steps of 10o for a total of 55-65 angles.
Probe beam of 350-750 nm at 60o incidence angle.
P-polarized pump beam: 35 fs pulses of 800 nm wavelength at 1 kHz repetition rate.
Delay time from -10 to 50 ps.
Time resolution of about 500 fs.
Sample Stage
Compensator
Analyzer
Polarizer
Pump Beam
Espinoza et al., APL 115, 052105 (2019).

## Slide 28
28
Semiconductors
Metal oxides
Bulk and thin films
Etc.
ELI Beamlines: ELI ERIC. Dolní Břežany (near Prague)
Second user call due April 25th, 2023: https://up.eli-laser.eu/
Contact Shirly Espinoza: shirly.espinoza@eli-beams.eu

## Slide 29
Ultrafast processes in photoexcited Germanium
1.55 eV pump beam creates N=1021 cm-3 electron-hole pairs near G-point. 9 mW power.
Heavy, light, split-off bands.
Ignore diffusion (for 1.55 eV pump).
Ignore Auger recombination.
Thermalization: Fermi-Dirac distribution
Intervalley scattering: G®X®L
Electrons accumulate at L.
Holes remain near G.
Electrons at L block E1 and E1+D1 transitions (Fermi-level singularity)
Bandgap renormalization: redshift expected
Lattice heating (25 K): redshift
Exciton screening
EF
Espinoza et al., APL 115, 052105 (2019).

## Slide 30
Ultrafast processes in photoexcited Germanium
1.55 eV pump beam creates N=4x1021 cm-3 electron-hole pairs near G-point.
The E1 and E1+D1 peaks decrease within the first two picoseconds and then recover: Band filling, excitonic screening followed by diffusion, Auger, and radiative recombination.
Maybe a Fermi level singularity near 2.6 eV.
Detailed modeling is required (Tanguy 2-D excitonic line shapes, including Fermi level singularity.)
Carlos Armenta, February 2023, unpublished.

## Slide 31
Ultrafast processes in photoexcited Germanium
1.55 eV pump beam creates N=4x1021 cm-3 electron-hole pairs near G-point.
The E1 and E1+D1 peaks decrease within the first two picoseconds and then recover. (Band filling, excitonic screening followed by diffusion, Auger, and radiative recombination)
Maybe a Fermi level singularity near 2.6 eV.
It looks like there is a redshift, but we need a line shape analysis with derivatives.
Carlos Armenta, February 2023, unpublished.

## Slide 32
Derivative analysis: critical point parameters
Carlos Armenta, February 2023, unpublished.
Emminger el al., PSS RRL 2022, 2200058.
Le, JVST B 37, 052903 (2019);
Extended Gauss filter
Filter width determined from Fourier coefficients

## Slide 33
Coherent acoustic phonon oscillations
Carlos Armenta, February 2023, unpublished.
Emminger el al., PSS RRL 2022, 2200058.
~19.5 meV
~5 meV
blueshift
redshift
Fermi singularity or strain ???

## Slide 34
Critical point parameters for E1 and E1+D1
Carlos Armenta, February 2023, unpublished.
Emminger el al., PSS RRL 2022, 2200058.
~19.5 meV
~5 meV
No red shift: phase angle changes. Where is BGR?
Phase shift

## Slide 35: Conclusions
Quantitative modeling of low-density optical processes is possible with basic physics and matrix elements from k.p theory:
  Photoluminescence in Ge
  Indirect gap absorption in Ge
  Direct gap absorption in Ge at low T
  More work is needed at high temperatures and for materials other than Ge.
High carrier excitations:
  High electron doping density in Ge
  Thermal excitation of electron-hole pairs in InSb
  Femtosecond laser generation of electron-hole pairs in Ge (ELI Beamlines)
  Experimental data and qualitative explanations exist
We need more experiments and more detailed theory and simulations.
Notes: Birstein-Moss shift

## Slide 36: Thank you! Questions?

## Slide 37: Direct band gap of InSb from 80 to 700 K
Measurement of the dielectric function of bulk InSb from 80 to 700 K near the direct band gap (E0)
Bulk InSb: Commercial (MTI), (100) orientation, undoped, n-type, rough back side
Direct Bandgap at 300 K: 0.17 eV

## Slide 38: Ellipsometry from 190 nm to 40,000 nm
Two different instruments are used for measurements from the mid-infrared to the deep ultraviolet spectral range.
J.A. Woollam IR-VASE
SZ, Spectroscopic Ellipsometry from 10 to 700 K, Adv. Opt. Technol. 11, 117 (2022).
J.A. Woollam V-VASE

## Slide 39: Temperature-dependent ellipsometry: 80-700 K
Using FTIR spectroscopic ellipsometry in an ultra-high vacuum (UHV) cryostat with CVD diamond windows (Janis ST-400, Diamond Materials GmbH, Freiburg).
Why diamond? Large transparency range and good vacuum seals, but expensive and high reflection losses.
J.A. Woollam IR-VASE
Energies: 30-40 meV to 1 eV
VIS-UV and FTIR spectra (dielectric functions) After oxide correction (25 Å)
Cryostat with CVD diamond windows
E0
Compare:
Aspnes, PRB 27, 985 (1983)
Logothetidis, PRB 31, 947 (1985).
Schaefer, JAP 127, 165705 (2020).
SZ, Adv. Opt. Technol. 11, 117 (2022).

## Slide 40: InSb (100) sample preparation (cleaning)
The InSb (100) sample was cleaned using water and isopropanol on the ultrasonic cleaner for 15 min on each to remove organic layers before the temperature dependent ellipsometry measurements.
Also: Anneal sample at 450 K in UHV overnight (degas)
Not used: BrM, HCl-methanol
(Aspnes/Studna 1983)
 | Oxide Thickness (Å)
Before Clean | 28.2
After Clean | 22.5
Oxide and organic layers
InSb

## Slide 41: InSb (100): Initial attempt was promising
Multiple experimental issues:
InSb sample cracks, melts, reacts with the Cu sample holder.
Adhesive (carbon nanoparticles, silver paint) expands, evaporates, redeposits on the windows.
Beam larger than sample: Depolarization from sample holder reflections.
Black-body radiation, heat shield.
Cryostat leaks, thermocouple breaks.
Initial result: Clear redshift with increasing temperature (up to 450 K).
Strange things happen above 450 K.

## Slide 42: Data and oxide corrections (4 years later)
InSb pseudo-dielectric Functions (“raw” data) from 80 to 800 K
= Bandgap
Band gap reduced with increasing temperature (but only below 500 K)
Drude response at high temperatures (thermally excited carriers)
Depolarization artifacts at long wavelengths (below 300 K)
SZ, Spectroscopic Ellipsometry from 10 to 700 K, Adv. Opt. Technol. 11, 117 (2022).

## Slide 43: Band gap analysis
How does the band gap of InSb change with temperature?
Tauc Plot:
Parametric-Semiconductor Model:
*manual extrapolation*
*Based on oscillator model*
Need linear region, not possible
C. M. Herzinger, B. Johs, et al., J. Appl. Phys. 83, 3323 (1998).

## Slide 44: Conclusions
Dielectric function of InSb measured from 80 to 700 K (with oxide correction of 25±5 Å)
Band gap is difficult to determine from a Tauc plot.
Parametric semiconductor model shows great results for the band gap.
Band gap shrinks with increasing temperature, but only up to 500 K.
Band gap stays constant near 550 K and then increases again to 700 K.
Drude tail due to thermal excitation of electron-hole pairs.
Carrier concentration and mobility is reasonable (compared to Hall measurements).
Detailed modeling requires Tanguy-Elliott theory of absorption by screened excitons, non-parabolicity, degenerate Fermi-Dirac statistics, k.p theory (in progress).
InSb would behave as a topological insulator above melting point. Not possible.
M. Rivero Arias et al., JVST B (submitted).
Notes: Birstein-Moss shift

## Slide 45: Sad ending
Unfortunately, the InSb sample melted at 750 K, but melting point is 800 K…
Cannot become a topological insulator because it melts.
Before
After
Future work:
Repeat experiment at high temperatures (below 750 K).
Increasing and decreasing temperature scans.
M. Rivero Arias et al., JVST B (submitted).