## Slide 1: Thin-Film and Powder Characterization with X-rays and Polarized Light
Stefan Zollner
Head, Department of Physics, New Mexico State University, Las Cruces, NM
Email: zollner@nmsu.edu. WWW: http://femto.nmsu.edu or http://research.nmsu.edu/ResearchCores/XRAY.html
PANalytical Empyrean XRD

## Slide 2: Thin Film and Powder Characterization
How thick is my film?
What are the film properties?
  Thickness, density, roughness (XRR)
  Band gap (Ellipsometry)
  Refractive index and absorption coefficient
  Infrared vibrations
  Strain and stress, alloy composition
  Lattice constants, crystal structure, position of the atoms in the cell
  Orientation, epitaxial alignment
  Temperature dependence of properties (10 to 800 K)
Powder and single-crystal characterization:
  Chemical identification from diffraction patterns (PDF data base)
  Lattice constants, crystal structure, position of the atoms in the cell
  Rietfeld refinement
2
GaAs
Ge1-ySny
Oxide

## Slide 3: Powder X-ray Diffraction (XRD)
3
Bragg’s Law

## Slide 4: High-Resolution and Single-Crystal X-ray Diffraction (HR-XRD)
4
GaAs
GeSn
1.2% Sn
GaAs
GeSn
2.6% Sn
High-Resolution Diffraction: Requires monochromatic and parallel x-ray beam
Suitable for highly crystalline epitaxial layers.
Symmetric and asymmetric reciprocal space maps
Example: Germanium-tin alloy on GaAs
Measure strain, lattice constant, and composition

## Slide 5: X-ray Reflectivity (XRR): Thickness, density, roughness
5
Oxide: 1.4 nm thick, 71% density, 0.4 nm rms
Si: 17.2 nm thick, 100% density (fixed), 3 nm rms
SiGe: 26% Ge (fixed), 95% density, 0.5 nm rms
epoxy
Si
SiGe
TEM: 16-17 nm thick. SIMS: 26% Ge. Raman: 75% strained.
For this smooth sample (0.6 nm rms) XRR gives excellent results.
Transmission electron micrograph

## Slide 6: Ellipsometry and Infrared Ellipsometry
6
Band gap of InAs
Infrared lattice vibrations in gallium phosphide
Temperature: 4-800 K

## Slide 7: Training and Education
7
Is it difficult to learn how to do this? No, but it takes practice (like violin or piano).
Interdisciplinary courses offered at NMSU
  PHYS 468/568: Elements of XRD
  PHYS 489/589: Modern Materials
  PHYS 471/571: Experimental Optics
  Intended for students from other majors with STEM background (C E, CHME, MAE).
Safety training by NMSU EHS&RM
Individual training by your research group.

## Slide 8: Thank you
Questions?