## Slide 1: Matrix elements and excitonic effects in the direct gap absorption of semiconductors
Stefan Zollner
in collaboration with:
Carola Emminger, Carlos A. Armenta, Sonam Yadav, Melissa Rivero Arias, Jaden Love (NMSU),
Jose Mendendez (Arizona State)
Department of Physics, New Mexico State University, Las Cruces, NM, USA
Email: zollner@nmsu.edu. WWW: http://femto.nmsu.edu.
LXVII Congreso Nacional de Física
Sociedad Mexicana de Física
Chihuahua, Mexico, 09 October 2024
FA9550-20-1-0135 AFOSR
FA9550-24-1-0061 AFOSR
NSF DMR-2235447 NSF

## Slide 2: New Mexico State University, Las Cruces
Stefan Zollner, SMF Congress, October 2024
Land grant institution, Carnegie R2 (soon to be R1) Comprehensive: Arts and Sciences, Education, Business, Agriculture
Ph.D. programs in sciences, engineering, agriculture; Ag extension; Chile Pepper Institute
12,700 students (11,000 UG, 1,700 GR), 1000 faculty
Minority-serving, Hispanic-serving (60% Hispanic/NA, 26% White)
Small-town setting (111,000)
Military-friendly institution (Army and Air Force ROTC programs)
Community engagement classification (first-generation students, Pell grant recipients)
Physics: BS/BA, MS, PhD degrees. 67 UG and 39 GR students.
11 faculty (HE Nuclear and Materials Physics), 2.4 M$ expenditures. ABET-accredited BS in Physics and BS in Engineering Physics

## Slide 3: Problem statement: Optical constants
(1) Achieve a quantitative understanding of photon absorption and emission processes.
Our qualitative understanding of excitonic absorption is 50-100 years old (Einstein coefficients),
But insufficient for modeling of detectors and emitters.
(2) How are optical processes affected by high carrier concentrations (screening)?
High carrier densities can be achieved with
  In situ doping
  ultrafast (femtosecond) lasers, see talk by Carlos Armenta today at 4:30pm
  high temperatures (narrow-gap or gapless semiconductors)
Application: CMOS-integrated mid-infrared camera (thermal imaging with a phone).

## Slide 4: Application: Midwave Infrared Detectors Germanium-Tin Alloys
4

## Slide 5: Spectroscopic ellipsometry
femto.nmsu.edu
UHV cryostat
& V-VASE ellipsometer
ellipsometric angles y, D
refractive index n+ik
dielectric function e
Tompkins & Hilfiker, Spectroscopic Ellipsometry (2016)

## Slide 6: Ellipsometry at NMSU
Stefan Zollner, 2023
Ellipsometry on anything (inorganic, 3D)
Metals, insulators, semiconductors
Mid-IR to vacuum UV (150 nm to 40 mm)
10 to 800 K, ultrafast ellipsometry
Ellipsometry tells us a lot about materials quality (not necessarily what we want to know).
diamond windows
closed-cycle He cooler
http://femto.nmsu.edu

## Slide 7: Matrix elements and excitonic effects in the direct gap absorption of semiconductors
Einstein coefficients, Fermi’s Golden Rule, Elliott-Tanguy excitons
Direct gap absorption in germanium from 10 to 800 K
Optical constants of highly excited semiconductors
  Direct gap absorption in InSb from 10 to 800 K
  Intravalence band absorption in topological insulators (a-tin)
  Optical constants of highly excited germanium (femtosecond ellipsometry at ELI Beamlines in Prague) – Carlos Armenta: 4:30pm.
Conclusion and Outlook
Stefan Zollner, SMF Congress, October 2024

## Slide 8: Einstein coefficients
Albert Einstein, Strahlungs-Emission und Absorption nach der Quantentheorie, DPG Verh. 18, 318 (1916); Phys. Z. 18, 121 (1917). See also Mark Fox.
A21
B12
B21
In equilibrium: N1, N2 constant. Absorption and emission balance.
Black-body radiation
One coefficient is sufficient:
Use Fermi’s Golden Rule to calculate B12

## Slide 9: Fermi’s Golden Rule: Tauc plot
Direct band gap absorption
Use k·p matrix element P: EP=2P2/m0
Fox, Chapter 3
constant k·p matrix element
Joint DOS
parabolic bands

## Slide 10: Fermi’s Golden Rule: Tauc plot
Direct band gap absorption
Use k·p matrix element P: EP=2P2/m0
The Tauc plot is wishful thinking.
No linear region:
Conduction band nonparabolicity
Broadening
1/E2 denominator.
excitons
Melissa Rivero Arias

## Slide 11: Exciton concept: Bound Electron-Hole Pair
Valence Band
Conduction Band
Energy
Ef
Ei
Eg
hω
e
Excitons in semiconductors
Conduction band
Valence band
e
Semiconductor Picture
Ground State
Exciton
Large radius (larger than atomic spacing)
Weakly bound
Bohr model for exciton
R
Fox, Chapter 4

## Slide 12: Bohr model for free excitons
Electron and hole form a bound state with binding energy.
RH=13.6 eV Rydberg energy.
QM mechanical treatment easy.
Reduced electron/hole mass (optical mass)
Static screening with static dielectric constant er.
Exciton radius: aH=0.53 Å
Excitons stable if R>>kT
Exciton momentum is zero.
Exciton enhancement important even if R<<kT (high temperature).
Fox, Chapter 4

## Slide 13: Sommerfeld enhancement
Excitonic Rydberg energy
Discrete states
Discrete absorption
Continuum absorption
R. J. Elliott, Phys. Rev. 108, 1384 (1957)
Yu & Cardona; Fox, Chapter 4
Use Bohr wave functions to calculate e2.
Toyozawa discusses broadening.

## Slide 14: Elliott-Tanguy exciton absorption
Direct band gap absorption
Excitonic binding energy: R=RH×mh/es2
´
bound excitons
exciton continuum enhancement
Tanguy’s contributions:
Add Lorentzian broadening
Kramers-Kronig transform to get the real part.
R. J. Elliott, Phys. Rev. 108, 1384 (1957).
Christian Tanguy, Phys. Rev. Lett. 75, 4090 (1995) + (E)

## Slide 15: Calculation of absorption spectrum from k·p theory
Can we calculate the absorption spectrum?
Yes, we can for Ge in the low carrier density limit.
It does not work for other III/V compounds.
Carola Emminger et al., JAP 131, 165701 (2022).

## Slide 16: Elliott-Tanguy theory applied to Ge
Fixed parameters:
  Electron and hole masses (temperature dependent)
  Excitonic binding energy R
  Amplitude A (derived from matrix element P)
Adjustable parameters:
  Broadening Γ: 2.3 meV
  Band gap E0
  Linear background A1 and B1 (contribution from E1 to real part of e)
  Problems:
  Broadening below the gap (band tail, oxide correction)
Carola Emminger et al., JAP 131, 165701 (2022).
ε1
ε2
Ge
10 K
16
Quantitative agreement

## Slide 17: Elliott-Tanguy theory applied to Ge
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
??? at high T.
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
17

## Slide 18: Elliott-Tanguy theory: problems for Ge at high T
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
Temperature dependence of the effective mass.
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
18

## Slide 19: Temperature dependence of the effective mass
19
Effective electron mass given by k·p theory
Temperature dependence of the direct band gap has two contributions:
  Thermal expansion of the lattice
  Electron-phonon interaction (Debye-Waller term and self-energy)
“Mass band gap” should only include the thermal expansion.
E0: direct band gap
k·p matrix element P: EP=2P2/m0
Self-energy
Thermal expansion
Total
Experiment
SZ, Solid State Commun. 77, 485 (1991).
P.B. Allen and M. Cardona, Phys. Rev. B 27 4760 (1983).
InSb

## Slide 20: Problem statement: Optical constants
(1) Achieve a quantitative understanding of photon absorption and emission processes.
Our qualitative understanding of excitonic absorption is 50-100 years old (Einstein coefficients),
But insufficient for modeling of detectors and emitters.
(2) How are optical processes affected by high carrier concentrations (screening)?
High carrier densities can be achieved with
  In situ doping
  ultrafast (femtosecond) lasers, see talk by Carlos Armenta today at 4:30pm
  high temperatures (narrow-gap or gapless semiconductors)
Application: CMOS-integrated mid-infrared camera (thermal imaging with a phone).

## Slide 21: Dielectric function of InSb from 80 to 800 K
Melissa Rivero Arias, JVSTB 41, 022203 (2023)
21
Band gap changes with temperature (but only below 500 K).
Amplitude reduction at high temperatures (Pauli blocking, bleaching)
Drude response at high temperatures (thermally excited carriers).
Depolarization artifacts at long wavelengths (below 300 K).
Woollam FTIR-VASE
cryostat with CVD diamond windows
InSb
InSb

## Slide 22: Band gap analysis for InSb
C. M. Herzinger, B. Johs, et al., J. Appl. Phys. 83, 3323 (1998)
Rivero Arias, JVSTB 41, 022203 (2023)
22
How does the band gap of InSb change with temperature?
Parametric-Semiconductor Model:
Also vary “shape parameters”.
Asymmetric peak shape poorly described.
Try Tanguy oscillator for excitonic line shape.
InSb

## Slide 23: Band gap of InSb from 80 to 800 K
23
Bose-Einstein Model
Band gap changes with temperature (but only below 500 K)
Described by Bose-Einstein model below 500 K: Logothetidis, PRB 31, 947 (1985).
No redshift above 500 K: Thermal Burstein-Moss shift
T.S. Moss, Proc. Phys. Soc. 67, 775 (1954).
E. Burstein, Phys. Rev. 93, 632 (1954).
InSb

## Slide 24: k·p theory (band structure method)
24
Stefan Zollner, 2023, AFRL Lectures Series 3
Schrödinger equation
Use Bloch’s theorem:
Solve equation for k=0.
Eliminate green free-electron term with substitution of variables (Kane 1957).
Then treat red term in perturbation theory.
Works very well for semiconductors with local V(r) potentials.
Yu & Cardona, Fundamentals of Semiconductors
Kane, J. Phys. Chem. Solids 1, 249 (1957). Kane 1966.
Product rule

## Slide 25: Nonparabolicity of InSb conduction band from k·p theory
25
Kane, J. Phys. Chem. Solids 1, 249 (1957).
Kane 8x8 k·p Hamiltonian:
Cubic characteristic equation:
Large spin-orbit approximation:
Energy versus k
(InSb)
Density of CB states

## Slide 26: Chemical potential in intrinsic InSb
S. Zollner and J. Menendez (unpublished).
26
Intrinsic condition: n=p.
Find chemical potential as a function of T.

## Slide 27: Chemical potential in intrinsic InSb
S. Zollner and J. Menendez (unpublished).
27
Intrinsic condition: n=p.
Find chemical potential as a function of T.
Degenerate Fermi-Dirac statistics.
Nonparabolicity of conduction band.

## Slide 28: Thermal excitations of electron-hole pairs in InSb
kBT=Eg/4 at 600 K
Fermi level above
conduction band edge above 450 K.
M. Rivero Arias et al., JVSTB 41, 022203 (2023).
Oswaldowski/Zimpel, J. Phys. Chem. Solids 49, 1179 (1988).
D. L. Rode, Phys. Rev. B 3, 3287 (1971).
28
n=2x1018 cm-3 at 800 K
Thermal Burstein-Moss shift
Drude response of free carriers
Reduction of absorption coefficient

## Slide 29: Condensation of excitons at high density
Exciton gas
Electron-hole liquid
Mott transition (insulator-metal) when electron separation equals exciton radius.
Electron separation d for density N
Mott transition occurs at rs near 1.
GaAs: n=1017 cm-3.
Biexciton, triexciton molecule formation.
Electron-hole droplets. Bose-Einstein condensation.
dimensionless
Fox, Chapter 4

## Slide 30: Excitons in doped or excited semiconductors
C. Tanguy, Phys. Rev. 60, 10660 (1999).
Banyai & Koch, Z. Phys. B 63, 283 (1986).
Need to include exciton screening due to doping.
Yukawa potential: Schrödinger equation not solvable.
Use Hulthen potential as an approximation
Coulomb
Yukawa
Hulthen
Hulthen exciton
Unscreened: g=∞
Fully screened: g=0
Mott criterion: g=1
Debye screening length

## Slide 31: Tanguy: Dielectric function of screened excitons
C. Tanguy, Phys. Rev. B 60, 10660 (1999)
Bound exciton states (finite number):
exciton continuum:
Need to introduce Lorentzian broadening and perform numerical KK transform.
Reduced Rydberg energy

## Slide 32: Tanguy: Dielectric function of screened excitons
Stefan Zollner, 2023, AFRL Lectures Series 3
g=∞
g=0
g=0
g=∞
g=1.5
g=0
(screened)
g=∞ (unscreened)
C. Tanguy, Phys. Rev. B 60, 10660 (1999)
Small Broadening
Large Broadening
g=∞
g=0

## Slide 33: Excitons in laser-excited GaAs
GaAs 300 K
High laser excitation
g=∞
g small
Haug and Koch, Quantum Theory of Optical and Electronic Properties of Semiconductors
Y. H. Lee, Phys. Rev. Lett 57, 2446 (1986)
Hulthen exciton

## Slide 34: Optical constants model: screened excitons
Absorption by screened excitons (Hulthen potential)
Degenerate Fermi-Dirac statistics to calculate fh and fe.
Numerical Kramers-Kronig transform (need occupation factors)
Two terms for light and heavy excitons
Non-parabolicity and temperature-dependent mass included from k.p theory
k-dependent matrix element P.
Screening parameter g=12/p2aRkTF (large: no screening) Sommerfeld enhancement persists well above the Mott density.
Only two free parameters: Band gap E0 and broadening G
Amplitude A and exciton binding energy R from k.p theory and effective masses
Christian Tanguy, Phys. Rev. B 60, 10660 (1999).
Jose Menendez, Phys. Rev. B 101, 195204 (2020).
Carola Emminger, J. Appl. Phys. 131, 165701 (2022).

## Slide 35: Relativistic Effects: Darwin Shift: C, Si, Ge, Sn
The s* band moves down, as the elements get heavier.
In a-tin, the s* band moves into the p-band manifold, between the j=1/2 and j=3/2 states.
This makes a-tin an (inverted) gapless semiconductor.
j=1/2
j=3/2
p

## Slide 36: Intravalence band absorption in gapless topological insulators (a-tin)
R.A. Carrasco, APL 113, 232104 (2018).
All gapless (inverted) semiconductors should have this peak.
Theory with same model as Ge IVB (Kaiser 1953, Kahn 1955).
looks like an exciton

## Slide 37: Simple 8x8 k·p band structure of a-tin (Kane)
S. Zollner, JVST B 42, 022203 (2024).
Kane 8x8 k·p Hamiltonian:
Cubic characteristic equation:
a-tin
dashed: parabolic
solid: nonparabolic

## Slide 38: Excitonic intravalence band absorption in a-tin
S. Zollner, JVST B 42, 022203 (2024).
without
excitons
with excitons
without
excitons
with excitons
Screening:
nonparabolicity affects exciton radius (screening)
Parabolic bands

## Slide 39: Conclusions
Quantitative modeling of low-density optical processes is possible with basic physics and matrix elements from k.p theory:
  Photoluminescence in Ge (Menendez)
  Indirect gap absorption in Ge (Menendez)
  Direct gap absorption in Ge at low T
  More work is needed at high temperatures and for materials other than Ge.
High carrier excitations:
  High electron doping density in Ge
  Thermal excitation of electron-hole pairs in InSb and a-tin.
  Femtosecond laser generation of electron-hole pairs in Ge (ELI Beamlines)
  Experimental data and qualitative explanations exist
We need more experiments and more detailed theory and simulations.
Notes: Birstein-Moss shift

## Slide 40: Thank you! Questions? Many students contributed to this project.
http://femto.nmsu.edu

## Slide 41
Biography
Regensburg/Stuttgart
Germany
NMSU
Las Cruces, NM
Since 2010
Motorola (Mesa, Tempe)
Arizona, 1997-2005
Motorola, Freescale
Texas, 2005-2007
Freescale, IBM
New York, 91-92; 07-10
41
Ames, IA

## Slide 42: Where is Las Cruces, NM ???
White Sands NP
Organ Mountains/Desert Peaks NM

## Slide 43: Ge Band structure: where did this come from?
Fox, Chapter 3
Works well for Ge, GaAs, etc.
Add kinetic energy
sp3 hybrid
Darwin shift
s2p2
y1+y2
y1-y2

## Slide 44: Critical points in the dielectric function of Ge
Peaks in the dielectric function
Due to interband transitions from valence to conduction band (electron-hole pairs)
P.Y. Yu and M. Cardona, Fundamentals of Semiconductors.

## Slide 45: Two-dimensional Bohr problem
Assume that m|| is infinite (separate term).
Use cylindrical coordinates.
Separate radial and polar variables.
Similar Laguerre solution as 3D Bohr problem.
M. Shinada and S. Sugano, J. Phys. Soc. Jpn. 21, 1936 (1966).
Half-integral quantum numbers
2D critical point

## Slide 46: Two-dimensional saddle-point excitons (E1, E1+D1)
B. Velicky and J. Sak, phys. status solidi 16, 147 (1966)
C. Tanguy, Solid State Commun. 98, 65 (1996)
W. Hanke and L.J. Sham, Phys. Rev. B 21, 4656 (1980)
Strong excitonic contribution to E1 critical point in Si (mot so much in Ge).

## Slide 47: Comparison with experimental data
Experimental data:
Emminger (5 K), JVST B 38, 012202 (2020).
Nunley (300 K),
JVST B 34,
061205 (2016)