## Slide 1: Accurate measurements and models of temperature-dependent optical constants for infrared detector materials
Stefan Zollner
With Carlos A. Armenta, Carola Emminger, Sonam Yadav, Melissa Rivero Arias, Jaden R. Love (NMSU), Jose Mendendez (Arizona State)
Department of Physics, New Mexico State University, Las Cruces, NM, USA
Email: zollner@nmsu.edu. WWW: http://femto.nmsu.edu.
2024 IEEE Photonics Conference (IPC) Rome, Italy, 10 - 14 Nov 2024
FA9550-20-1-0135 AFOSR
FA9550-24-1-0061 AFOSR
DMR-2235447 NSF
DMR-2423992 NSF
Ge

## Slide 2: Precision measurements of optical constants
Bulk materials: Semiconductors, metals, insulators SiC, SrTiO3, AlSb, Ge, GaAs, GaP, GaSb, InSb, SiC (4H and 6H), Ni, Pt, Au, MgAl2O4, NiO (excitons), LiF, LSAT, ZnGa2O4, LaAlO3
Epitaxial layers (CVD, MBE, ALD): NbO2, Co3O4, SrTiO3 (doped, quantum wells), BaSnO3, ZnO, SnO2,HfO2, GdxGa2-xO3, silicides, SiGe:C, GeSn, GaAs1-xPx, alpha-tin on InSb and CdTe, native oxides on semiconductors (GeO2)
Comparison with ab initio density functional theory and with k.p theory (Jose Menendez)
Ellipsometry measurements over a broad spectral range (30 meV to 9.5 eV) and broad temperature range (4 K to 800 K). Also femtosecond time resolution (ELI Beamlines).
Applications: Microelectronics industry (CMOS, bipolar, III/V), mid-wave infrared detectors
WWW: http://femto.nmsu.edu

## Slide 3: Spectroscopic ellipsometry
femto.nmsu.edu
UHV cryostat
& V-VASE ellipsometer
ellipsometric angles y, D
refractive index n+ik
dielectric function e
Tompkins & Hilfiker, Spectroscopic Ellipsometry (2016)

## Slide 4: Ellipsometry at NMSU
Stefan Zollner, 2023
Ellipsometry on anything (inorganic, 3D)
Metals, insulators, semiconductors
Mid-IR to vacuum UV (150 nm to 40 mm)
10 to 800 K, ultrafast ellipsometry
Ellipsometry tells us a lot about materials quality (not necessarily what we want to know).
diamond windows
closed-cycle He cooler
http://femto.nmsu.edu

## Slide 5: Problem statement: optical constants
(1) Achieve a quantitative understanding of photon absorption and emission processes.
Our qualitative understanding of excitonic absorption is 50-100 years old (Einstein coefficients),
But insufficient for modeling of detectors and emitters.
(2) How are optical processes affected by high carrier concentrations (screening)?
High carrier densities can be achieved with
  In situ doping (Menendez, Kouvetakis)
  high temperatures (narrow-gap or gapless semiconductors)
  ultrafast (femtosecond) lasers
Application: CMOS-integrated mid-infrared camera (thermal imaging with a phone).

## Slide 6: Application: Midwave Infrared Detectors Germanium-Tin Alloys
6

## Slide 7: Einstein coefficients
Albert Einstein, Strahlungs-Emission und Absorption nach der Quantentheorie, DPG Verh. 18, 318 (1916); Phys. Z. 18, 121 (1917). See also Mark Fox.
A21
B12
B21
In equilibrium: N1, N2 constant. Absorption and emission balance.
Black-body radiation
One coefficient is sufficient:
Use Fermi’s Golden Rule to calculate B12

## Slide 8: Fermi’s Golden Rule: Tauc plot
Direct band gap absorption
Use k·p matrix element P: EP=2P2/m0
Fox, Chapter 3
constant k·p matrix element
Joint DOS
parabolic bands
The Tauc plot is wishful thinking.
excitons

## Slide 9: Fermi’s Golden Rule: Tauc plot
Direct band gap absorption
Use k·p matrix element P: EP=2P2/m0
The Tauc plot is wishful thinking.
No linear region:
Conduction band nonparabolicity
Broadening
1/E2 denominator.
excitons
Melissa Rivero Arias

## Slide 10: Bohr model for free excitons
Electron and hole form a bound state with binding energy.
RH=13.6 eV Rydberg energy.
QM mechanical treatment easy.
Reduced electron/hole mass (optical mass)
Static screening with static dielectric constant er.
Exciton radius: aH=0.53 Å
Excitons stable if R>>kT
Exciton momentum is zero.
Exciton enhancement important even if R<<kT (high temperature).
Fox, Chapter 4

## Slide 11: Sommerfeld enhancement (3D)
Excitonic Rydberg energy
Discrete states
Discrete absorption
Continuum absorption
R. J. Elliott, Phys. Rev. 108, 1384 (1957)
Yu & Cardona; Fox, Chapter 4; Tanguy 1995
Use Bohr wave functions to calculate e2.
Toyozawa discusses broadening.

## Slide 12: Elliott-Tanguy exciton absorption
Direct band gap absorption
Excitonic binding energy: R=RH×mh/es2
´
bound excitons
exciton continuum enhancement
Tanguy’s contributions:
Add Lorentzian broadening
Kramers-Kronig transform to get the real part.
R. J. Elliott, Phys. Rev. 108, 1384 (1957).
Christian Tanguy, Phys. Rev. Lett. 75, 4090 (1995) + (E)

## Slide 13
13

## Slide 14: Elliott-Tanguy theory applied to Ge
Fixed parameters:
  Electron and hole masses (temperature dependent)
  Excitonic binding energy R
  Amplitude A (derived from matrix element P)
Adjustable parameters:
  Broadening Γ: 2.3 meV
  Band gap E0
  Linear background A1 and B1 (contribution from E1 to real part of e)
  Problems:
  Broadening below the gap (band tail, oxide correction)
Carola Emminger et al., JAP 131, 165701 (2022).
ε1
ε2
Ge
10 K
14
Quantitative agreement

## Slide 15: Elliott-Tanguy theory applied to Ge
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
??? at high T.
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
15

## Slide 16: Elliott-Tanguy theory: problems for Ge at high T
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
Temperature dependence of the effective mass.
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
16

## Slide 17: Temperature dependence of the effective mass
17
Effective electron mass given by k·p theory
Temperature dependence of the direct band gap has two contributions:
  Thermal expansion of the lattice
  Electron-phonon interaction (Debye-Waller term and self-energy)
“Mass band gap” should only include the thermal expansion.
E0: direct band gap
k·p matrix element P: EP=2P2/m0
Self-energy
Thermal expansion
Total
Experiment
SZ, Solid State Commun. 77, 485 (1991).
P.B. Allen and M. Cardona, Phys. Rev. B 27 4760 (1983).
InSb

## Slide 18: Two-dimensional saddle-point excitons (E1, E1+D1)
B. Velicky and J. Sak, phys. status solidi 16, 147 (1966)
W. Hanke and L.J. Sham, Phys. Rev. B 21, 4656 (1980)
C. Tanguy, Solid State Commun. 98, 65 (1996)
Strong excitonic contribution to E1 critical point in Si (mot so much in Ge).

## Slide 19: Two-dimensional Bohr problem
Assume that m|| along (111) is infinite (separate term).
Use cylindrical coordinates.
Separate radial and polar variables.
Similar Laguerre solution as 3D Bohr problem.
M. Shinada and S. Sugano, J. Phys. Soc. Jpn. 21, 1936 (1966). Flügge (Rechenmethoden QM, 1952).
Half-integral quantum numbers
2D critical point
(same as in 3D)

## Slide 20: Two-dimensional excitons at E1 critical points of Ge
Peak at for
with
C. Tanguy, SSC 98, 65 (1996).
preliminary

## Slide 21: Problem statement: optical constants
(1) Achieve a quantitative understanding of photon absorption and emission processes.
Our qualitative understanding of excitonic absorption is 50-100 years old (Einstein coefficients),
But insufficient for modeling of detectors and emitters.
(2) How are optical processes affected by high carrier concentrations (screening)?
High carrier densities can be achieved with
  In situ doping (Menendez, Kouvetakis; Arizona State University)
  high temperatures (narrow-gap or gapless semiconductors)
  ultrafast (femtosecond) lasers
Application: CMOS-integrated mid-infrared camera (thermal imaging with a phone).

## Slide 22: Condensation of excitons at high density
Exciton gas
Electron-hole liquid
Mott transition (insulator-metal) when electron separation equals exciton radius.
Electron separation d for density N
Mott transition occurs at rs near 1.
GaAs: n=1017 cm-3.
Biexciton, triexciton molecule formation.
Electron-hole droplets. Bose-Einstein condensation.
dimensionless
Fox, Chapter 4

## Slide 23: Excitons in doped or excited semiconductors
C. Tanguy, Phys. Rev. 60, 10660 (1999).
Banyai & Koch, Z. Phys. B 63, 283 (1986). Haug & Koch (2009).
Need to include exciton screening due to doping.
Yukawa potential: Schrödinger equation not solvable.
Use Hulthen potential as an approximation
Coulomb
Yukawa
Hulthen
Hulthen exciton
Unscreened: g=∞
Fully screened: g=0
Mott criterion: g=1
Debye screening length

## Slide 24: Tanguy: Dielectric function of screened excitons
C. Tanguy, Phys. Rev. B 60, 10660 (1999)
Bound exciton states (finite number):
exciton continuum:
Need to introduce Lorentzian broadening and perform numerical KK transform.
Reduced Rydberg energy

## Slide 25: Tanguy: Dielectric function of screened excitons
Stefan Zollner, 2023, AFRL Lectures Series 3
g=∞
g=0
g=0
g=∞
g=1.5
g=0
(screened)
g=∞ (unscreened)
C. Tanguy, Phys. Rev. B 60, 10660 (1999)
Small Broadening
Low Temp
Large Broadening
High Temp
g=∞
g=0

## Slide 26: k·p theory (band structure method)
26
Stefan Zollner, 2023, AFRL Lectures Series 3
Schrödinger equation
Use Bloch’s theorem:
Solve equation for k=0.
Eliminate green free-electron term with substitution of variables (Kane 1957).
Then treat red term in perturbation theory.
Works very well for semiconductors with local V(r) potentials.
Yu & Cardona, Fundamentals of Semiconductors
Kane, J. Phys. Chem. Solids 1, 249 (1957). Kane 1966.
Product rule

## Slide 27: Relativistic Effects: Darwin Shift: C, Si, Ge, Sn
The s* band moves down, as the elements get heavier.
In a-tin, the s* band moves into the p-band manifold, between the j=1/2 and j=3/2 states.
This makes a-tin an (inverted) gapless semiconductor.
j=1/2
j=3/2
p

## Slide 28: Intravalence band absorption in gapless topological insulators (a-tin)
R.A. Carrasco, APL 113, 232104 (2018).
All gapless (inverted) semiconductors should have this peak.
Theory with same model as Ge IVB (Kaiser 1953, Kahn 1955).
looks like an exciton

## Slide 29: Simple 8x8 k·p band structure of a-tin (Kane)
S. Zollner, JVST B 42, 022203 (2024).
Kane 8x8 k·p Hamiltonian:
Cubic characteristic equation:
a-tin
dashed: parabolic
solid: nonparabolic

## Slide 30: Excitonic intravalence band absorption in a-tin
S. Zollner, JVST B 42, 022203 (2024).
without
excitons
with excitons
without
excitons
with excitons
Screening:
nonparabolicity affects exciton radius (screening)
Parabolic bands

## Slide 31: Dielectric function of InSb from 80 to 800 K
Melissa Rivero Arias, JVSTB 41, 022203 (2023)
31
Band gap changes with temperature (but only below 500 K).
Amplitude reduction at high temperatures (Pauli blocking, bleaching)
Drude response at high temperatures (thermally excited carriers).
Depolarization artifacts at long wavelengths (below 300 K).
Woollam FTIR-VASE
cryostat with CVD diamond windows
InSb
~0.2 eV band gap
InSb

## Slide 32: Optical constants model: screened excitons
Absorption by screened excitons (Hulthen potential)
Degenerate Fermi-Dirac statistics to calculate fh and fe.
Numerical Kramers-Kronig transform (need occupation factors)
Two terms for light and heavy excitons
Non-parabolicity and temperature-dependent mass included from k.p theory
k-dependent matrix element P.
Screening parameter g=12/p2aRkTF (large: no screening) Sommerfeld enhancement persists well above the Mott density.
Only two free parameters: Band gap E0 and broadening G
Amplitude A and exciton binding energy R from k.p theory and effective masses
Christian Tanguy, Phys. Rev. B 60, 10660 (1999).
Jose Menendez, Phys. Rev. B 101, 195204 (2020).
Carola Emminger, J. Appl. Phys. 131, 165701 (2022).

## Slide 33: Band gap analysis for InSb
C. M. Herzinger, B. Johs, et al., J. Appl. Phys. 83, 3323 (1998)
Melissa Rivero Arias, JVSTB 41, 022203 (2023)
33
How does the band gap of InSb change with temperature?
Parametric-Semiconductor Model:
Also vary “shape parameters”.
Asymmetric peak shape poorly described.
Try Tanguy oscillator for excitonic line shape.
InSb

## Slide 34: Band gap of InSb from 80 to 800 K
34
Bose-Einstein Model
Band gap changes with temperature (but only below 500 K)
Described by Bose-Einstein model below 500 K: Logothetidis, PRB 31, 947 (1985).
No redshift above 500 K: Thermal Burstein-Moss shift
T.S. Moss, Proc. Phys. Soc. 67, 775 (1954).
E. Burstein, Phys. Rev. 93, 632 (1954).
InSb

## Slide 35: Nonparabolicity of InSb conduction band from k·p theory
35
Kane, J. Phys. Chem. Solids 1, 249 (1957).
Kane 8x8 k·p Hamiltonian:
Cubic characteristic equation:
Large spin-orbit approximation:
Energy versus k
(InSb)
Density of CB states

## Slide 36: Femtosecond Pump-Probe Ellipsometry
Probe
Pump
H. Kalt, Semiconductor Optics 2 (2024).
Tompkins & Hilfiker, Spectroscopic Ellipsometry (2016)
Non-linear effects in germanium induced by photoexcited carriers:
Screening (many-body)
Carrier-carrier scattering.
Carrier-phonon scattering.
Intervalley scattering.
Momentum and energy relaxation of hot carriers.
1

## Slide 37: Experimental setup: pump-probe ellipsometry
Ch: Chopper (500 Hz, 250 Hz)
A: Analyzer
P: Polarizer
CR: Rotating Compensator
L: Lens
S: Sample
DL: Delay Line (~6.67 ns pump-probe delay, 3 fs resolution)
BS: Beam Splitter
SCG: Super-continuum Generation
CCD: Charge-coupled device detector
S. Richter, Rev. Sci. Instrum. 92, 033104 (2021).
S. Espinoza, Appl. Phys. Lett. 115, 052105 (2019).
1.55 eV pump beam path
White light probe beam path
Eli Beamlines
Dolni Brezany, Czech Republic
35 fs

## Slide 38: Set-up: Femtosecond pump-probe ellipsometry
Rotating compensator ellipsometer:
Compensator was rotated in steps of 10o for a total of 55-65 angles.
Probe beam of 350-750 nm at 60o incidence angle.
P-polarized pump beam: 35 fs pulses of 800 nm wavelength at 1 kHz repetition rate.
Delay time from -10 to 50 ps.
Time resolution of about 500 fs.
Espinoza et al., APL 115, 052105 (2019).
Sample Stage
Compensator
Analyzer
Polarizer
Pump
Probe
Focusing lens
Eli Beamlines
Dolni Brezany, Czech Republic

## Slide 39
Pseudo-dielectric constant as function of delay time
Rapid decrease of e within first 500 fs.
Recovery takes 1 ns or longer.
500 fs
Carlos A. Armenta, Shirly J. Espinoza (unpublished)

## Slide 40
2D excitons with band filling - no screening
No screening included for 2D excitons

## Slide 41: Band-filling effects
We combine Tanguy’s line shape for 2D excitons with Xu’s band-filling model:
cm-3
cm-3
Simulation of the chemical potential as a function of temperature for different carrier densities.
C. Xu, J. Appl. Phys. 125, 085704 (2019).
C. Xu, Phys. Rev. Lett. 118, 267402 (2017).
No screening included for 2D excitons
Carlos A. Armenta, Shirly J. Espinoza (unpublished)

## Slide 42: Summary: Screening of excitons
Excitonic direct gap absorption: 3D hydrogen problem with Coulomb potential treated in every quantum mechanics course Sommerfeld enhancement of the absorption.
Screened exciton absorption: 3D hydrogen problem with Yukawa potential Not solvable analytically, use Hulthen potential (Banyai & Koch, Haug & Koch) Sommerfeld enhancement persists well above the Mott transition.
Excitonic direct gap absorption in 2D materials or E1 excitons 2D hydrogen problem with Coulomb potential (Flügge: Rechenmethoden der QM)
Excitonic 2D-transitions at E1 with screening (femtosecond ellipsometry) No known solution for screened Sommerfeld enhancement in 2D.

## Slide 43: Conclusions
Quantitative modeling of low-density optical processes is possible with basic physics and matrix elements from k.p theory:
  Photoluminescence in Ge (Menendez)
  Indirect gap absorption in Ge (Menendez)
  Direct gap absorption in Ge at low T (excitons in 3D); E1 critical points in Ge (excitons in 2D)
  More work is needed at high temperatures and for materials other than Ge.
High carrier excitations:
  High electron doping density in Ge
  Thermal excitation of electron-hole pairs in InSb and a-tin (3D screening and band filling).
  Femtosecond laser generation of electron-hole pairs in Ge (2D screening)
  Experimental data and qualitative explanations exist
We need more experiments and more detailed theory and simulations.
Notes: Birstein-Moss shift

## Slide 44: Thank you! Questions? Many students contributed to this project.
http://femto.nmsu.edu

## Slide 45
Biography
Regensburg/Stuttgart
Germany
NMSU
Las Cruces, NM
Since 2010
Motorola (Mesa, Tempe)
Arizona, 1997-2005
Motorola, Freescale
Texas, 2005-2007
Freescale, IBM
New York, 91-92; 07-10
45
Ames, IA

## Slide 46: Where is Las Cruces, NM ???
White Sands NP
Organ Mountains/Desert Peaks NM

## Slide 47: Ge Band structure: where did this come from?
Fox, Chapter 3
Works well for Ge, GaAs, etc.
Add kinetic energy
sp3 hybrid
Darwin shift
s2p2
y1+y2
y1-y2

## Slide 48: Critical points in the dielectric function of Ge
Peaks in the dielectric function
Due to interband transitions from valence to conduction band (electron-hole pairs)
P.Y. Yu and M. Cardona, Fundamentals of Semiconductors.

## Slide 49: Two-dimensional Bohr problem
Assume that m|| is infinite (separate term).
Use cylindrical coordinates.
Separate radial and polar variables.
Similar Laguerre solution as 3D Bohr problem.
M. Shinada and S. Sugano, J. Phys. Soc. Jpn. 21, 1936 (1966).
Half-integral quantum numbers
2D critical point

## Slide 50: Two-dimensional saddle-point excitons (E1, E1+D1)
B. Velicky and J. Sak, phys. status solidi 16, 147 (1966)
C. Tanguy, Solid State Commun. 98, 65 (1996)
W. Hanke and L.J. Sham, Phys. Rev. B 21, 4656 (1980)
Strong excitonic contribution to E1 critical point in Si (mot so much in Ge).

## Slide 51: Comparison with experimental data
Experimental data:
Emminger (5 K), JVST B 38, 012202 (2020).
Nunley (300 K),
JVST B 34,
061205 (2016)

## Slide 52: Optical Absorption at High Carrier Densities
Intense femtosecond laser excitation (ELI Beamlines) (electrons pile at L-point)
High n-doping of Ge with P
(free electrons pile up at L-point)
Xu et al., PRL 118, 267402 (2017)
High temperature
(thermal excitation of e-h pairs)
constant m and E0
InSb
Rivero, JVSTB 41, 022203 (2023)
Espinoza, APL 115, 052105 (2019)
52