## Slide 1: Matrix elements and excitonic effects in the direct gap absorption of semiconductors
Stefan Zollner
with:
Carola Emminger (Uni Leipzig and HU Berlin, Germany)
Jose Menendez (Arizona State University, Tempe, AZ)
College of Arts and Sciences, Department of Physics
New Mexico State University, Las Cruces, NM, USA
2024 Nebraska Ellipsometry Lecture Mini Series
FA9550-20-1-0135 AFOSR
NSF DMR-2235447 NSF
Email: zollner@nmsu.edu. WWW: http://femto.nmsu.edu.

## Slide 2
Biography
Regensburg/Stuttgart
Germany
NMSU
Las Cruces, NM
Since 2010
Motorola (Mesa, Tempe)
Arizona, 1997-2005
Motorola, Freescale
Texas, 2005-2007
Freescale, IBM
New York, 91-92; 07-10
2

## Slide 3: Where is Las Cruces, NM ???
White Sands NP

## Slide 4: New Mexico State University, Las Cruces
Stefan Zollner, 2023
Land grant institution, Carnegie R2 (soon to be R1) Comprehensive: Arts and Sciences, Education, Business, Agriculture
Ph.D. programs in sciences, engineering, agriculture; Ag extension
14,000 students (11,500 UG, 2,500 GR), 1000 faculty
Minority-serving, Hispanic-serving (60% Hispanic/NA, 26% White)
Small-town setting
Military-friendly institution (Army and Air Force ROTC programs)
Community engagement classification (first-generation students, Pell grant recipients)
Physics: BS/BA, MS, PhD degrees. 71 UG and 37 GR students.
12 faculty (HE Nuclear and Materials Physics), 1.7 M$ expenditures. ABET-accredited BS in Physics and BS in Engineering Physics

## Slide 5: Ellipsometry at NMSU
Stefan Zollner, 2023
Ellipsometry on anything (inorganic, 3D)
Metals, insulators, semiconductors
Mid-IR to vacuum UV
10 to 800 K
Ellipsometry tells us a lot about materials quality (not necessarily what we want to know).
diamond windows
closed-cycle He

## Slide 6: Problem statement
(1) Achieve a quantitative understanding of absorption and emission processes.
Our qualitative understanding of excitonic absorption is 50-100 years old,
But insufficient for modeling of detectors and emitters.
(2) How are optical processes affected by high carrier concentrations (screening)?
High carrier densities can be achieved with
  In situ doping or
  ultrafast (femtosecond) lasers or
  high temperatures (narrow-gap or gapless semiconductors)
Goal: CMOS-integrated mid-infrared camera (thermal imaging with a phone).
Future: How are optical processes affected by an electric field (pin diode or thin layer)?
Stefan Zollner, Fall 2023 MRS Meeting

## Slide 7
7

## Slide 8: Matrix elements and excitonic effects in the direct gap absorption of semiconductors
Einstein coefficients, Fermi’s Golden Rule, Elliott-Tanguy excitons
Direct gap absorption in germanium from 10 to 800 K
Optical constants of highly excited semiconductors
  Direct gap absorption in InSb from 10 to 800 K
  Intravalence band absorption in topological insulators (a-tin)
  Optical constants of highly excited germanium (femtosecond ellipsometry at ELI Beamlines in Prague) – Carlos Armenta F’24.
Conclusion and Outlook
Stefan Zollner, Fall 2023 MRS Meeting

## Slide 9: Einstein coefficients
Albert Einstein, Strahlungs-Emission und Absorption nach der Quantentheorie, DPG Verh. 18, 318 (1916); Phys. Z. 18, 121 (1917). See also Mark Fox.
A21
B12
B21
In equilibrium: N1, N2 constant. Absorption and emission balance.
Black-body radiation
One coefficient is sufficient:
Use Fermi’s Golden Rule to calculate B12

## Slide 10: Fermi’s Golden Rule: Tauc plot
Direct band gap absorption
Use k·p matrix element P: EP=2P2/m0
Fox, Chapter 3
constant k·p matrix element
Joint DOS
parabolic bands

## Slide 11: Fermi’s Golden Rule: Tauc plot
Direct band gap absorption
Use k·p matrix element P: EP=2P2/m0
The Tauc plot is wishful thinking.
No linear region:
Conduction band nonparabolicity
Broadening
1/E2 denominator.
excitons
Melissa Rivero Arias

## Slide 12: Elliott-Tanguy exciton absorption
Direct band gap absorption
Excitonic binding energy: R=RH×mh/es2
´
bound excitons
exciton continuum enhancement
Tanguy’s contributions:
Add Lorentzian broadening
Kramers-Kronig transform to get the real part.
R. J. Elliott, Phys. Rev. 108, 1384 (1957).
Christian Tanguy, Phys. Rev. Lett. 75, 4090 (1995) + (E)

## Slide 13: Calculation of absorption spectrum from k·p theory
Can we calculate the absorption spectrum?
Yes, we can for Ge in the low carrier density limit.
It does not work for other III/V compounds.
Carola Emminger et al., JAP 131, 165701 (2022).

## Slide 14: Elliott-Tanguy theory applied to Ge
Fixed parameters:
  Electron and hole masses (temperature dependent)
  Excitonic binding energy R
  Amplitude A (derived from matrix element P)
Adjustable parameters:
  Broadening Γ: 2.3 meV
  Band gap E0
  Linear background A1 and B1 (contribution from E1 to real part of e)
  Problems:
  Broadening below the gap (band tail, oxide correction)
Carola Emminger et al., JAP 131, 165701 (2022).
ε1
ε2
Ge
14
Quantitative agreement

## Slide 15: Elliott-Tanguy theory applied to Ge
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
??? at high T.
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
15

## Slide 16: Elliott-Tanguy theory: problems for Ge at high T
Good agreement at low temperatures.
Model also describes second derivatives.
Potential problems:
Matrix element k-dependent
Nonparabolicity
Resonant indirect absorption
Temperature dependence of the effective mass.
Carola Emminger et al., JAP 131, 165701 (2022).
Ge
Ge
16

## Slide 17: Temperature dependence of the effective mass
17
Effective electron mass given by k·p theory
Temperature dependence of the direct band gap has two contributions:
  Thermal expansion of the lattice
  Electron-phonon scattering (Debye-Waller term and self-energy)
“Mass band gap” should only include the thermal expansion.
TBD: Polaron effects on effective mass in III/V materials.
E0: direct band gap
k·p matrix element P: EP=2P2/m0
Self-energy
Thermal expansion
Total
Experiment
SZ, Solid State Commun. 77, 485 (1991).
P.B. Allen and M. Cardona, Phys. Rev. B 27 4760 (1983).
InSb

## Slide 18: Optical Absorption at High Carrier Densities
Intense femtosecond laser excitation (ELI Beamlines) (electrons pile at L-point)
High n-doping of Ge with P
(free electrons pile up at L-point)
Xu et al., PRL 118, 267402 (2017)
High temperature
(thermal excitation of e-h pairs)
constant m and E0
InSb
Rivero, JVSTB 41, 022203 (2023)
Espinoza, APL 115, 052105 (2019)
18
Stefan Zollner, Fall 2023 MRS Meeting

## Slide 19: (1) Dielectric function of InSb from 80 to 800 K
Rivero Arias, JVSTB 41, 022203 (2023)
19
Band gap changes with temperature (but only below 500 K).
Amplitude reduction at high temperatures (Pauli blocking, bleaching)
Drude response at high temperatures (thermally excited carriers).
Depolarization artifacts at long wavelengths (below 300 K).
Woollam FTIR-VASE
cryostat with CVD diamond windows
InSb
InSb

## Slide 20: Band gap analysis for InSb
C. M. Herzinger, B. Johs, et al., J. Appl. Phys. 83, 3323 (1998)
Rivero Arias, JVSTB 41, 022203 (2023)
20
How does the band gap of InSb change with temperature?
Parametric-Semiconductor Model:
Also vary “shape parameters”.
Asymmetric peak shape poorly described.
Try Tanguy oscillator for excitonic line shape.
InSb

## Slide 21: Band gap of InSb from 80 to 800 K
21
Bose-Einstein Model
Band gap changes with temperature (but only below 500 K)
Described by Bose-Einstein model below 500 K: Logothetidis, PRB 31, 947 (1985).
No redshift above 500 K: Thermal Burstein-Moss shift
T.S. Moss, Proc. Phys. Soc. 67, 775 (1954).
E. Burstein, Phys. Rev. 93, 632 (1954).
InSb

## Slide 22: k·p theory (band structure method)
22
Stefan Zollner, 2023, AFRL Lectures Series 3
Schrödinger equation
Use Bloch’s theorem:
Solve equation for k=0.
Eliminate green free-electron term with substitution of variables (Kane 1957).
Then treat red term in perturbation theory.
Works very well for semiconductors with local V(r) potentials.
Yu & Cardona, Fundamentals of Semiconductors
Kane, J. Phys. Chem. Solids 1, 249 (1957). Kane 1966.
Product rule

## Slide 23: Nonparabolicity of InSb conduction band from k·p theory
23
Kane, J. Phys. Chem. Solids 1, 249 (1957).
Kane 8x8 k·p Hamiltonian:
Cubic characteristic equation:
Large spin-orbit approximation:
Energy versus k
Density of CB states

## Slide 24: Chemical potential in intrinsic InSb
S. Zollner and J. Menendez (unpublished).
24
Intrinsic condition: n=p.
Find chemical potential as a function of T.

## Slide 25: Chemical potential in intrinsic InSb
S. Zollner and J. Menendez (unpublished).
25
Intrinsic condition: n=p.
Find chemical potential as a function of T.
Degenerate Fermi-Dirac statistics.
Nonparabolicity of conduction band.

## Slide 26: Thermal excitations of electron-hole pairs in InSb
kBT=Eg/4 at 600 K
Fermi level above
conduction band edge above 450 K.
M. Rivero Arias et al., JVSTB 41, 022203 (2023).
Oswaldowski/Zimpel, J. Phys. Chem. Solids 49, 1179 (1988).
D. L. Rode, Phys. Rev. B 3, 3287 (1971).
26
n=2x1018 cm-3 at 800 K
Thermal Burstein-Moss shift
Drude response of free carriers
Reduction of absorption coefficient

## Slide 27: Optical constants model: screened excitons
Absorption by screened excitons (Hulthen potential)
Degenerate Fermi-Dirac statistics to calculate fh and fe.
Numerical Kramers-Kronig transform (need occupation factors)
Two terms for light and heavy excitons
Non-parabolicity and temperature-dependent mass included from k.p theory
k-dependent matrix element P.
Screening parameter g=12/p2aRkTF (large: no screening) Sommerfeld enhancement persists well above the Mott density.
Only two free parameters: Band gap E0 and broadening G
Amplitude A and exciton binding energy R from k.p theory and effective masses
Christian Tanguy, Phys. Rev. B 60, 10660 (1999).
Jose Menendez, Phys. Rev. B 101, 195204 (2020).
Carola Emminger, J. Appl. Phys. 131, 165701 (2022).

## Slide 28: Relativistic Effects: Darwin Shift: C, Si, Ge, Sn
The s* band moves down, as the elements get heavier.
In a-tin, the s* band moves into the p-band manifold, between the j=1/2 and j=3/2 states.
This makes a-tin an (inverted) gapless semiconductor.
j=1/2
j=3/2
p

## Slide 29: Intravalence band absorption in gapless topological insulators (a-tin)
R.A. Carrasco, APL 113, 232104 (2018).
All gapless (inverted) semiconductors should have this peak.
Theory with same model as Ge IVB (Kaiser 1953, Kahn 1955).
looks like an exciton

## Slide 30: Simple 8x8 k·p band structure of a-tin (Kane)
S. Zollner, JVST 2024 (in print).
Kane 8x8 k·p Hamiltonian:
Cubic characteristic equation:
a-tin
dashed: parabolic
solid: nonparabolic

## Slide 31: Excitonic intravalence band absorption in a-tin
Parabolic bands
nonparabolicity affects exciton radius (screening)
without
excitons
with excitons
without
excitons
with excitons
Screening:
S. Zollner, JVST 2024 (in print).

## Slide 32
Thickness dependence of excitonic absorption
ZnO on Si with different thicknesses.
This might be an electric field effect.
(Samarasingha, Sudeshna Chattopadhyay, SZ, JVSTB 2020)
Fox, Chapter 4
Field ionization

## Slide 33: Conclusions
Quantitative modeling of low-density optical processes is possible with basic physics and matrix elements from k.p theory:
  Photoluminescence in Ge (Menendez)
  Indirect gap absorption in Ge (Menendez)
  Direct gap absorption in Ge at low T
  More work is needed at high temperatures and for materials other than Ge.
High carrier excitations:
  High electron doping density in Ge
  Thermal excitation of electron-hole pairs in InSb and a-tin.
  Femtosecond laser generation of electron-hole pairs in Ge (ELI Beamlines)
  Experimental data and qualitative explanations exist
We need more experiments and more detailed theory and simulations.
Notes: Birstein-Moss shift

## Slide 34: Thank you! Questions? Many students contributed to this project.