## Slide 1: Measurements of temperature-dependent optical constants and comparison with theory
Stefan Zollner
Department of Physics
New Mexico State University Las Cruces, NM, USA
Email: zollner@nmsu.edu.
WWW: http://femto.nmsu.edu
10th International Conference on Spectroscopic Ellipsometry (ICSE-10) Boulder, CO, USA, 8-13 June 2025
FA9550-20-1-0135 AFOSR
FA9550-24-1-0061 AFOSR
FA9453-23-2-0001 AFRL
DMR-2235447 NSF
DMR-2423992 NSF

## Slide 2: Where is Las Cruces, NM ???
White Sands NP

## Slide 3: Students and Collaborators (2010-2025)
PhD. students (10): Lina S. Abdallah, Nalin Fernando, Nuwanjula S. Samarasingha, Farzin Abadizaman, Carola Emminger, Rigo A. Carrasco, Yoshitha Hettige, Carlos A. Armenta, Sonam Yadav, Beata Hroncova.
MS students (5): Travis I. Willett-Gies, Cesar A. Rodriguez, Jaden R. Love, Haley B. Woolf, Aaron Lopez Gonzalez.
Undergraduate students (22): Amber A. Medina, Maria Spies, Cayla M. Nelson, Eric DeLong, Christian J. Zollner, Khadijih N. Mitchell, Ayana Ghosh, T. Nathan Nunley, Laura G. Pineda, Luis A. Barrera, Dennis P. Trujillo, Jaime M. Moya, Jacqueline A. Cooke, Alexandra P. Hartmann, Cesy M. Zamarripa, Zachary Yoder, Pablo P. Paradis, Melissa Rivero Arias, Atlantis K. Moses, Danissa P. Ortega, Gabriel Ruiz, Meghan Worrell.
Ellipsometry collaborators: Jose Menendez (Arizona State), Arnold M. Kiefer (AFRL/RY), Mathias Schubert (Nebraska), Premysl Marsik (Fribourg), Christian Bernhard (Fribourg), Igal Brener (Sandia), Wim Geerts (Texas State), Tom Tiwald (JAW), Preston Webster (AFRL/RV), Martin Veis, Jan Hrabovsky (Charles University), Dagmar Chvostova, Alexandr Dejneka, Marina Tyunina (IOP/CAS).
Thin-film epitaxial samples from many different sources: Arizona State, Delaware, Texas, IIT Indore, Texas State, AFRL/RY+RV, Arkansas, Sandia, NREL, NASA, SOITEC, QuantTera, Connecticut, IBM, Global Foundries, UNM, Ohio State, etc.
Stefan Zollner, ICSE-10 2025, Boulder, CO

## Slide 4: ICSE Conference Topics
Instrumentation to acquire ellipsometric angles, Jones matrices, or MM elements.
Analysis of ellipsometry data to determine (isotropic or anisotropic) optical constants.
Ellipsometry as a non-destructive characterization tool: How thick is my film?
Fundamental mechanisms of light-matter interactions.
What can the dielectric function tell us about a material?
1993 (Paris), 1997 (Charleston, SC, USA), 2003 (Vienna), 2007 (Stockholm), 2010 (Albany), 2013 (Kyoto), 2016 (Berlin), 2019 (Barcelona), 2022 (Beijing), 2025 (Boulder, CO, USA)
S. Zollner in Ellipsometry at the Nanoscale ed. by M. Losurdo and K. Hingerl (Springer, Heidelberg, 2013), p. 607-627.
Stefan Zollner, ICSE-10 2025, Boulder, CO

## Slide 5: Electromagnetic Spectrum
Infrared:
Lattice vibrations (phonons), free carriers (Drude response)
Visible and UV: Valence electrons, electronic band structure (electrons, holes, interband transitions, critical points)
X-rays: Core electrons; Gamma-rays: Nuclear processes
Stefan Zollner, ICSE-10 2025, Boulder, CO
An electromagnetic wave interacts with positive and negative charges through the Coulomb force.

## Slide 6: Outline: Infrared Response of Crystalline Solids
Lorentz model for absorption by optical phonons in polar crystals.
  Trends with mass and ionicity.
Temperature dependence of optical phonon energies:
  Anharmonic decay of optical phonons.
  Two-phonon absorption in LiF and NiO.
Beyond the Lorentz model: Frequency-dependent decay rate
  Lowndes model (TO/LO oscillator).
Splitting of optical phonons in uniaxial crystals: ZnO, SiC, NiO
Multimode behavior in GaAs1-xPx alloys
Berreman effect at LO energy: Insulator on metal (LiF on Ag)
Drude model for free carrier absorption: Ni and Au
Plasmon-phonon coupling.

## Slide 7
q
Lorentz Model for Oscillating Charges
Charge density
Resonance frequency
H. Helmholtz, Ann. Phys 230, 582 (1875)
F. Wooten, Optical Properties of Solids, 1972
dipole moment
Static screening.
Friction proportional to velocity.
Small displacement (harmonic).

## Slide 8
Lorentz Model for Oscillating Charges
wLO=1290 cm-1
e(w) shows symmetric TO resonance peak.
Loss function Im(-1/e) peaks at LO frequency.
TO
LO
TO
LO
F. Wooten, Optical Properties of Solids, 1972
M. Schubert, Infrared Ellipsometry, 2004
Ionic bond

## Slide 9: GaP shows nearly perfect Lorentz oscillator
Reststrahlen
Band
e∞=9.14
es=15.7
Loss function
epsilon
psi
Delta
364.9 cm-1
402.5 cm-1
N. Samarasingha,
JVSTB 39, 052201 (2021)

## Slide 10: Infrared Lattice Vibrations (Lorentz model)
N. Samarasingha,
JVSTB 39, 052201 (2021)

## Slide 11: Why Temperature-Dependent Ellipsometry ???
SZ, Spectroscopic ellipsometry from 10 to 700 K,
Adv. Opt. Techn. 11, 117 (2022).
Practical applications: Optical devices at low or high T.
Peaks get sharper at low temperature (easier to detect).
Thermal expansion is trivial (usually small contribution).
Finite lifetime: Quality factor decreases (broadening increases).
Temperature decreases the lifetime.
Damped oscillator is broader and has lower energy then undamped oscillator.
Temperature dependence yields energy of decay product and strength of interaction (complex self energy).
Distinguish intrinsic lifetime (homogeneous) broadening from inhomogenous broadening (disorder, defects, alloy, etc).
Inhomogeneous broadening does not change with temperature.
Phase transitions (Ni Curie temperature, phase change materials).
L. Viña et al., PRB 30, 1979 (1984).

## Slide 12: Tools for Temperature-Dependent Ellipsometry
Jaden Love
Atlantis Moses
ARO (W911NF-22-2-0130)
Closed-cycle system works well.
Vibrations do not seem to be a problem.
Ongoing issue: Thin ice layer forms on sample (even in UHV).
Window calibration is important.
Custom feature: Diamond windows for cryostat.

## Slide 13: Tools for Temperature-Dependent Ellipsometry
Jaden Love
Atlantis Moses

## Slide 14: Temperature dependence of GaP phonon energies
GaP
Anharmonic phonon decay: TO, LO -> TA + LA
Broadenings increase.
TO and LO energies decrease.
Born effective charge: constant.
es, e¥ increase (Penn gap)
N. Samarasingha et al., JVSTB 39, 052201 (2021)
Zunger PRB 1999

## Slide 15: Two-phonon absorption in LiF and NiO
Willett-Gies & Nelson, JVST A 33, 061202 (2015).
Also Humlicek TSF 313-314, 687 (1998).
Small absorption in the reststrahlen band causes a dip or terrace.
Compare also with Al, Cu, Au (Fox, Optical Properties of Metals).

## Slide 16
Two-Phonon Absorption in NiO
Rocksalt crystal structure (FCC), Space group 225 (Fm-3m).
Single TO/LO phonon pair: G15
Antiferromagnetic ordering along (111), causes phonon splitting (8-30 cm-1).
Second-order phonon absorption.
TO
TA+TO phonon
NiO Reststrahlen Band
Rooksby, Nature, 1943
es=11.3
e¥=5.0
Willett-Gies & Nelson,
JVST A 33, 061202 (2015)
NiO cell
Absorption in the reststrahlen band
16

## Slide 17: Temperature Dependence of Two-Phonon Absorption
TO energy (49.6 meV) > 25.4 meV > TA(X) energy (16.5 meV)
Yoshitha Hettige
(ICSE-10)
NiO
NiO
NiO

## Slide 18: Frequency-Dependent Decay Rate
GaP
300 K
Lorentz oscillator: constant g
N. Samarasingha et al., JVSTB 39, 052201 (2021).
E. Baron et al., Phys. Rev. Mater. 3, 104603 (2019).
GaN
300 K
Difficult to evaluate because of noise.
gTO>gLO
gTO>gLO

## Slide 19: Frequency-Dependent Decay Rate: TO-LO
Berreman and Unterwald, Phys. Rev. 174, 791 (1968)
Lowndes, Phys. Rev. B 1, 2754 (1970)
Gervais and Piriou, J. Phys. C Solid State Phys. 7, 2374 (1974).
N. Samarasingha et al., JVSTB 39, 052201 (2021).
MSE=1.6
MSE=1.2
gTO=gLO
gTO>gLO
Simplest case: Two different broadening parameters for TO and LO phonons.
Or a complex Lorentzian amplitude.

## Slide 20: Frequency-Dependent Scattering Rate
Anharmonic decay of optical phonons into acoustic phonons (TO, LO -> LA +TA phonon).
Frequency dependent decay rate: gTO>gLO.
TO phonon absorption coefficient becomes negative above LO energy (dotted line).
How do we fix this? The two-phonon absorption also contributes to the absorption, keeping the total absorption coefficient positive.
gTO>gLO
N. Samarasingha et al., JVSTB 39, 052201 (2021).

## Slide 21: Reststrahlen Band in Uniaxial Crystal ZnO
Uniaxial crystal: Ordinary and extraordinary dielectric function.
Aspnes 1980: For c-axis oriented crystal, we measure the ordinary dielectric function (e>>1).
Assumption breaks down near the LO frequency where e is near zero.
4H-SiC
300 K
T. E. Tiwald et al., PRB 60, 11464 (1999).
N. Samarasingha et al., JVSTB 39, 052201 (2021).
Also: E. Franke et al., APL 70, 1668 (1997).

## Slide 22
No Phonon Anisotropy in c-axis NiO (111)cubic
Rocksalt Crystal Structure (FCC), Space Group 225 (Fm-3m).
Single TO/LO phonon pair.
Antiferromagnetic ordering along (111), should cause phonon splitting (8-30 cm-1).
Anisotropy not visible in NiO (111).
TO
NiO Reststrahlen Band
Rooksby, Nature, 1943
es=11.3
e¥=5.0
Willett-Gies & Nelson,
JVST A 33, 061202 (2015)
NiO cell
Phonon anisotropy is too small to be visible in NiO (111).
22

## Slide 23: Compare NiO (111) and (100)
NiO (111)
Isotropic
NiO (100)
Anisotropic

## Slide 24: Two-phonon absorption in LiF
Willett-Gies & Nelson, JVST A 33, 061202 (2015).
Also Humlicek TSF 313-314, 687 (1998).
Small absorption in the reststrahlen band causes a dip or terrace.
Compare also with Al, Cu, Au (Fox, Optical Properties of Metals).
Phonon energies in LiF:
TO: 304 cm-1
LO: 669 cm-1
LO phonon not seen in e2.
Ellipsometry only sees the TO phonon in bulk crystals.

## Slide 25: Berreman Effect: LiF on Ag
J. Humlicek, PSSB 215, 155 (1999).
Light is a transverse wave:
only couples to TO phonons.
cannot excite LO phonons.
TO: peak in e2.
LO: peak in loss function.
However: Interference effects cause structures at the LO phonon energy in thin films.
That’s called the Berreman effect.
LO
LO

## Slide 26: Multimode Behavior in Semiconductor Alloys
SZ et al., Appl. Phys. Lett. 123, 172102 (2023).
GaAs1-xPx alloys have four phonons:
2 TO, 2 LO.
Phonons cannot mix.
Energy pap between GaAs and GaP modes.
Some dependence of phonon energies on composition.
Vegard’s Law does not hold.
Two-mode behavior.

## Slide 27: Berreman Effect in Semiconductor Alloys
SZ et al., Appl. Phys. Lett. 123, 172102 (2023).
GaAs1-xPx alloys (on GaAs substrate) have four phonons:
2 TO, 2 LO.
Two reststrahlen bands:
GaAs-like (TO, LO)
GaP-like (TO, LO)
Berreman mode: LO phonon of GaAs substrate shows up in ellipsometry spectra
LO phonons (of substrate or layer) are seen in many ellipsometry spectra of thin films.

## Slide 28: Drude Response of Metals
F. Abadizaman and SZ, JVSTB 37, 062920 (2019).
Cleaning of surface (heating in UHV) is very important to obtain accurate results.
For a metal, psi should be 45 degrees up to VUV region.
Lowered because of interband transitions (more important for Ni because of partially filled d bands).
Why does psi never reach 45 degrees at low energies? Needs to be investigated. Anomalous skin effect?
Ni, 300 K
Au, 300 K

## Slide 29: Dielectric Function of Metals (Drude Response)
-e1, e2 very large in IR.
Interband transitions in UV range.
Better representation of data with optical conductivity: s=-ie0w(e-1)
F. Abadizaman and SZ, JVSTB 37, 062920 (2019).
Ni, 300 K
Au, 300 K

## Slide 30: Drude Response of Ni (Temperature-dependent)
Fitting the dielectric function of Ni:
Two Drude terms (s-, d-electrons)
Four Lorentz oscillators for interband transitions.
s=-ie0w(e-1)
F. Abadizaman, Jaden Love,
and SZ, JVSTA 40, 033202 (2022).
d-electrons
s-electrons

## Slide 31: Singularity at the Curie Temperature of Ni
A
Energy of interband transition at 4.8 eV shows typical redshift with increasing temperature.
Broadening decreases and shows singular behavior at the Curie temperature (similar to magnetization).
Tc
Tc
Two transitions merge into one above Tc.
F. Abadizaman, Jaden Love, and SZ, JVSTA 40, 033202 (2022).

## Slide 32: Plasmon-Phonon Coupling
A
A. A. Kukharskii, Solid-State Commun. 13, 1761 (1973).
SZ, JVSTB 37, 012904 (2019).
Also see posters by Daniel Franta.
Free carriers are longitudinal excitations, cannot mix with TO phonons.
Look at the loss function! Also, broadening.
7E16 cm-3
7E17 cm-3
7E16 cm-3
7E17 cm-3
LP
UP
LP
UP
LO mode couples with free carrier plasmon
to form
lower and upper
plasmon-phonon polaritons.

## Slide 33: Summary and Outlook
Lorentz model for absorption by optical phonons in polar crystals.
  Trends with mass and ionicity.
Temperature dependence of optical phonon energies:
  Anharmonic decay of optical phonons.
  Two-phonon absorption in LiF and NiO.
Beyond the Lorentz model: Frequency-dependent decay rate
  Lowndes model (TO/LO oscillator).
Splitting of optical phonons in uniaxial crystals: ZnO, SiC, NiO
Multimode behavior in GaAs1-xPx alloys
Berreman effect at LO energy: Insulator on metal (LiF on Ag)
Drude model for free carrier absorption: Ni and Au
Plasmon-phonon coupling

## Slide 34: Thank you! Questions?
PhD. students (10): Lina S. Abdallah, Nalin Fernando, Nuwanjula S. Samarasingha, Farzin Abadizaman, Carola Emminger, Rigo A. Carrasco, Yoshitha Hettige, Carlos A. Armenta, Sonam Yadav, Beata Hroncova.
MS students (5): Travis I. Willett-Gies, Cesar A. Rodriguez, Jaden R. Love, Haley B. Woolf, Aaron Lopez Gonzalez.
Undergraduate students (22): Amber A. Medina, Maria Spies, Cayla M. Nelson, Eric DeLong, Christian J. Zollner, Khadijih N. Mitchell, Ayana Ghosh, T. Nathan Nunley, Laura G. Pineda, Luis A. Barrera, Dennis P. Trujillo, Jaime M. Moya, Jacqueline A. Cooke, Alexandra P. Hartmann, Cesy M. Zamarripa, Zachary Yoder, Pablo P. Paradis, Melissa Rivero Arias, Atlantis K. Moses, Danissa P. Ortega, Gabriel Ruiz, Meghan Worrell.
Ellipsometry collaborators: Jose Menendez (Arizona State), Arnold M. Kiefer (AFRL/RY), Mathias Schubert (Nebraska), Premysl Marsik (Fribourg), Christian Bernhard (Fribourg), Igal Brener (Sandia), Wim Geerts (Texas State), Tom Tiwald (JAW), Preston Webster (AFRL/RV), Martin Veis, Jan Hrabovsky (Charles University), Dagmar Chvostova, Alexandr Dejneka, Marina Tyunina (IOP/CAS).
Thin-film epitaxial samples from many different sources: Arizona State, Delaware, Texas, IIT Indore, Texas State, AFRL/RY+RV, Arkansas, Sandia, NREL, NASA, SOITEC, QuantTera, Connecticut, IBM, Global Foundries, UNM, Ohio State, etc.

## Slide 35
Einstein Coefficients for Interaction Processes
Albert Einstein, Strahlungs-Emission und Absorption nach der Quantentheorie, DPG Verh. 18, 318 (1916); Phys. Z. 18, 121 (1917).
A21
B12
B21
In equilibrium: N1, N2 constant. Absorption and emission balance.
Black-body radiation
One coefficient is sufficient:
Use Fermi’s Golden Rule to calculate B12